LTSA599

ISO18752-DC Super Artery Steel Wire Spiral Hose

- Hose Construction

- Inner Tube:CR/NBR synthetic rubber

- Reinforcement:Multi-spiraled high tensile super flexible steel wire,
Four plies ≥ 1 million impulse cycles

- Outer Layer:Skiving-free abrasion and weather resistant synthetic rubber

- Temperature Range:-40°C to +120°C (-40°F  +248°F) -55°C  +100°C (-67°F to +212°F)

- Application:Remarkable performance on tight bend radius, high pressure,long service life, and high impulse,weather resistant for more than five years and warrantied for two years with Letone hose fittings and HNBR seals.Widely apply to excavator and other heavy duty construction machinery or hash working environment.

| SIZE |  | I.D |  | O.D |  | O.D |  | MAX.W.P | P.P | MIN.B.R |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Min | Max | Min | Max |  |  |  |
|  |  | mm | mm | mm | mm | mm | mm | MPa | MPa | mm |
| 10-4 | 3/8" | 9.5 | 10.5 | 17.8 | 19.0 | 20.5 | 22.5 | 56 | 224 | 100 |
| 13-4 | 1/2" | 12.5 | 13.5 | 19.8 | 21.0 | 21.8 | 23.8 | 42 | 168 | 140 |
| 16-4 | 5/8" | 15.9 | 16.6 | 23.9 | 25.1 | 26.0 | 28.0 | 42 | 168 | 180 |
| 19-4 | 3/4" | 18.8 | 19.6 | 27.9 | 29.1 | 30.0 | 32.0 | 42 | 168 | 200 |
| 25-4 | 1" | 25.0 | 25.8 | 34.4 | 36.4 | 36.8 | 39.2 | 42 | 168 | 250 |
| 32-4 | 1 1/4" | 31.6 | 32.6 | 40.9 | 42.9 | 43.3 | 45.7 | 35 | 140 | 400 |
| 38-4 | 1 1/2" | 37.8 | 38.8 | 48.1 | 50.1 | 51.3 | 53.7 | 32 | 128 | 480 |
| 51-4 | 2" | 50.7 | 52 | 62.6 | 63.8 | 65.6 | 67.4 | 25 | 100 | 650 |
| 32-6 | 1 1/4" | 31.6 | 32.6 | 46.4 | 48.4 | 49.0 | 51.4 | 42 | 168 | 400 |
| 38-6 | 1 1/2" | 37.7 | 38.8 | 52.0 | 54.0 | 54.8 | 57.0 | 42 | 168 | 480 |
| 51-6 | 2" | 50.7 | 52 | 66.4 | 67.6 | 69.1 | 70.9 | 42 | 168 | 630 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT599

ISO18752-CC Artery Wire Spiral Hydraulic Hose

- Hose Construction

- Inner Tube:NBR synthetic rubber

- Reinforcement:Four or six plies of spiraled high tensile steel wire,tested with 800,000 impulse cycles without leakage

- Outer Layer:Skiving-free abrasion and weather resistant synthetic rubber

- Temperature Range:-40°C to +120°C (-40°F to +248°F) -55°C to +100°C (-67°F to +212°F)

- Application:Remarkable performance on high pressure and high impulse. Widely apply to excavator and other heavy duty construction machinery.

| SIZE | ImperialStandard | Metric Specifications | I.D |  | W.D |  | O.D |  | MAX.W.P | P.P | MIN.B.P | MIN.Impulse | MIN.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SIZE | SIZE | MIN | MAX | MIN | MAX | MIN | MAX |  |  |  | 10k |  |  |
|  | DASH | IN | MM | MM | MM | MM | MM | MM | MPA | MPA | MPA | CYCLES | MM | Kg/m |
| -4 | 1/4-4S | 6.2 | 6.0 | 6.8 | 15.0 | 16.2 | 18.0 | 20.0 | 69 | 138 | 276 | 50 | 120 | 0.60 |
| -6 | 3/8-4S | 10 | 9.5 | 10.5 | 17.8 | 19.0 | 20.5 | 22.5 | 56 | 112 | 224 | 50 | 150 | 0.71 |
| -8 | 1/2-4S | 12.5 | 12.8 | 13.5 | 19.8 | 21.0 | 21.8 | 23.8 | 42 | 84 | 168 | 80 | 190 | 0.82 |
| -10 | 5/8-4S | 16 | 15.9 | 16.6 | 23.9 | 25.1 | 26.0 | 28.0 | 42 | 84 | 168 | 80 | 200 | 1.15 |
| -12 | 3/4-4S | 19 | 18.8 | 19.6 | 27.9 | 29.1 | 30.0 | 32.0 | 42 | 84 | 168 | 80 | 224 | 1.56 |
| -16 | 1-4S | 25 | 25.0 | 25.8 | 34.4 | 36.4 | 36.8 | 39.2 | 42 | 84 | 168 | 80 | 272 | 2.13 |
| -20 | 1 1/4-4S | 31.5 | 31.6 | 32.6 | 40.9 | 42.9 | 43.3 | 45.7 | 35 | 70 | 140 | 80 | 370 | 2.56 |
| -24 | 1 1/2-4S | 38 | 37.8 | 38.8 | 48.1 | 50.1 | 51.3 | 53.7 | 32 | 64 | 128 | 80 | 540 | 3.18 |
| -32 | 2-4S | 51 | 50.7 | 52 | 62.6 | 63.8 | 65.6 | 67.4 | 25 | 50 | 100 | 80 | 660 | 4.46 |
| -20 | 1 1/4-6S | 31.5 | 31.6 | 32.6 | 46.0 | 48.0 | 48.8 | 51.2 | 42 | 84 | 168 | 80 | 420 | 4.07 |
| -24 | 1 1/2-6S | 38 | 37.7 | 38.8 | 52.0 | 54.0 | 54.8 | 57.2 | 42 | 84 | 168 | 80 | 500 | 4.63 |
| -32 | 2-6S | 51.5 | 51.6 | 51.8 | 66.4 | 67.6 | 69.1 | 70.9 | 42 | 84 | 168 | 80 | 650 | 6.32 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT588

EN 856-4SH | MSHA | MA Wire Spiral Hydraulic Hose

- Hose Construction

- Inner Tube:Black oil resistant synthetic rubber

- Reinforcement:Four plies of spiraled high tensile steel wire

- Outer Layer:Black oil and weather resistant synthetic rubber

- Temperature Range:-40°C to +100°C (-40°F  +212°F)

- Application:Suitable for conveying water-based,petroleum-based, and biodegradable hydraulic oil.

| Specification | Specification | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -10 | 5/8 | 15.5 | 16.7 | 23.9 | 25.1 | 26.0 | 28.0 | 45 | 90 | 180 | 250 | 1.15 |
| -12 | 3/4 | 18.6 | 19.8 | 27.6 | 29.2 | 30.0 | 32.0 | 42 | 84 | 168 | 280 | 1.54 |
| -16 | 1 | 25.0 | 26.4 | 34.4 | 36.0 | 37.0 | 39.0 | 38 | 76 | 152 | 340 | 2.02 |
| -20 | 1 1/4 | 31.4 | 33.0 | 40.9 | 42.9 | 43.8 | 46.2 | 32.5 | 65 | 130 | 460 | 2.48 |
| -24 | 1 1/2 | 37.7 | 39.3 | 48.1 | 50.1 | 51.3 | 53.7 | 29 | 58 | 116 | 560 | 3.18 |
| -32 | 2 | 50.4 | 52.0 | 62.2 | 64.2 | 65.3 | 67.7 | 25 | 50 | 100 | 700 | 4.46 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT583

EN856-4SP|MSHA Wire Spiral Hydraulic Hose

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:four plies of spiraled high tensile steel wire

- Outer Layer:black oil and weather resistant synthetic rubber

- Temperature Range:-40°C  +100°C (-40°F  +212°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.

| SIZE | SIZE | I.D |  | W.D |  | 0.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -4 | 1/4 | 6.2 | 7.0 | 14.3 | 15.5 | 16.6 | 18.6 | 45 | 90 | 180 | 150 | 0.60 |
| -6 | 3/8 | 9.5 | 10.5 | 16.9 | 18.1 | 19.1 | 21.1 | 44.5 | 89 | 178 | 180 | 0.71 |
| -8 | 1/2 | 12.5 | 13.5 | 19.8 | 21.0 | 21.8 | 23.8 | 41.5 | 83 | 166 | 230 | 0.82 |
| -10 | 5/8 | 15.5 | 16.7 | 23.0 | 24.6 | 25.4 | 27.4 | 35 | 70 | 140 | 250 | 1.01 |
| -12 | 3/4 | 18.6 | 19.8 | 27.4 | 29.0 | 30.0 | 32.0 | 35 | 70 | 140 | 300 | 1.43 |
| -16 | 1 | 25.0 | 26.4 | 34.5 | 36.1 | 37.0 | 39.0 | 32 | 64 | 128 | 340 | 1.97 |
| -20 | 11/4 | 31.4 | 33.0 | 45.0 | 46.4 | 47.4 | 49.8 | 21 | 42 | 84 | 460 | 2.96 |
| -24 | 11/2 | 37.7 | 39.3 | 50.9 | 52.3 | 53.8 | 56.2 | 18.5 | 37 | 74 | 560 | 3.42 |
| -32 | 2 | 50.4 | 52.0 | 64.3 | 66.3 | 66.9 | 69.3 | 16.5 | 33 | 66 | 660 | 4.77 |

LT581

SAE 100R12|MSHA Wire Spiral Hydraulic Hose

- Hose Construction

- Inner Tube:black hot oil resistant synthetic rubber

- Reinforcement:four plies of spiraled high tensile steel wire

- Outer Layer:black oil and weather resistant synthetic rubber

- Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil under harsh working conditions.

| SIZE | SIZE | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -6 | 3/8 | 9.5 | 10.5 | 16.9 | 18.1 | 19.0 | 21.0 | 28 | 56 | 112 | 125 | 0.71 |
| -8 | 1/2 | 12.5 | 13.5 | 20.1 | 21.3 | 22.1 | 24.1 | 28 | 56 | 112 | 180 | 0.85 |
| -10 | 5/8 | 15.5 | 16.7 | 24.0 | 25.2 | 26.5 | 28.5 | 28 | 56 | 112 | 200 | 1.06 |
| -12 | 3/4 | 18.6 | 19.8 | 26.9 | 28.4 | 29.1 | 31.1 | 28 | 56 | 112 | 240 | 1.33 |
| -16 | 1 | 25.0 | 26.4 | 34.2 | 35.8 | 36.3 | 38.7 | 28 | 56 | 112 | 300 | 1.83 |
| -20 | 11/4 | 31.4 | 33.0 | 42.9 | 44.9 | 45.3 | 47.7 | 21 | 42 | 84 | 420 | 2.67 |
| -24 | 11/2 | 37.7 | 39.3 | 49.4 | 51.4 | 52.3 | 54.7 | 17.5 | 35 | 70 | 500 | 3.12 |
| -32 | 2 | 50.8 | 52.0 | 62.5 | 64.8 | 65.1 | 68.3 | 17.5 | 35 | 70 | 640 | 4.48 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT582

SAE 100R13|MSHA Wire Spiral Hydraulic Hose

- Hose Construction

- Inner Tube:black hot oil resistant synthetic rubber

- Reinforcement:four or six plies of spiraled high tensile steel wire

- Outer Layer:black oil and weather resistant synthetic rubber

- Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil under harsh working conditions.

| SIZE | SIZE | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -12 | 3/4 | 18.6 | 19.8 | 28.2 | 29.4 | 31.2 | 33.2 | 35 | 70 | 140 | 240 | 1.61 |
| -16 | 1 | 25.0 | 26.4 | 34.8 | 36.4 | 37.3 | 39.7 | 35 | 70 | 140 | 300 | 2.06 |
| -20 | 11/4 | 31.4 | 31.4 | 46.0 | 48.0 | 48.8 | 51.2 | 35 | 70 | 140 | 420 | 3.84 |
| -24 | 11/2 | 37.7 | 37.7 | 53.0 | 55.0 | 55.8 | 58.2 | 35 | 70 | 140 | 500 | 4.60 |
| -32 | 2 | 50.4 | 50.4 | 67.1 | 69.1 | 69.5 | 72.5 | 35 | 70 | 140 | 640 | 6.61 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT585

MT/T98|MSHA Wire Spiral Hydraulic Hose For Mining

- Hose Construction:

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:four or six plies of spiraled high tensile steel wire

- Outer Layer:black oil,weather, and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying medium like mineral oil,water-based hydraulic oil,or water in coal mining machinery such as coal mining hydraulic supportand coal shearer.

| Specification | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| 3/8-4 | 9.5 | 10.5 | 18.2 | 19.8 | 22.4 | 24.4 | 70 | 105 | 210 | 180 | 0.90 |
| 1/2-4 | 12.5 | 13.5 | 21.4 | 23.0 | 25.2 | 27.2 | 57 | 86 | 172 | 210 | 1.05 |
| 5/8-4 | 15.7 | 16.6 | 25.2 | 26.8 | 29.0 | 31.0 | 53 | 80 | 160 | 260 | 1.40 |
| 3/4-4 | 18.7 | 19.8 | 29.2 | 30.4 | 33.0 | 35.0 | 46 | 69 | 140 | 280 | 1.75 |
| 7/8-4 | 21.7 | 22.8 | 31.7 | 32.9 | 36.0 | 38.0 | 41 | 62 | 124 | 320 | 1.93 |
| 1-4 | 24.7 | 25.8 | 35.2 | 36.4 | 38.8 | 41.2 | 35 | 53 | 112 | 360 | 2.14 |
| 11/4-4 | 31.6 | 32.6 | 43.2 | 44.6 | 46.8 | 49.2 | 32 | 48 | 84 | 460 | 2.82 |
| 11/2-4 | 37.7 | 38.8 | 49.8 | 51.8 | 54.3 | 56.7 | 25 | 38 | 75 | 560 | 3.41 |
| 13/4-4 | 44.7 | 45.8 | 56.8 | 58.8 | 61.5 | 64.5 | 21 | 32 | 64 | 640 | 4.03 |
| 2-4 | 50.5 | 52.0 | 62.8 | 64.8 | 65.0 | 67.4 | 21 | 32 | 64 | 720 | 4.43 |
| 3/8-6 | 9.5 | 10.5 | 20.0 | 22.0 | 24.0 | 26.0 | 80 | 120 | 240 | 180 | 1.20 |
| 1/2-6 | 12.5 | 13.5 | 23.4 | 24.6 | 26.5 | 28.5 | 72 | 108 | 216 | 210 | 1.40 |
| 5/8-6 | 15.7 | 16.6 | 28.0 | 30.0 | 31.5 | 34.5 | 70 | 105 | 204 | 260 | 2.10 |
| 3/4-6 | 18.7 | 19.8 | 32.0 | 34.0 | 35.5 | 37.5 | 60 | 90 | 180 | 280 | 2.47 |
| 7/8-6 | 21.7 | 22.8 | 35.0 | 37.0 | 39.5 | 42.5 | 53 | 80 | 160 | 320 | 2.80 |
| 1-6 | 24.7 | 25.8 | 38.0 | 39.6 | 41.8 | 44.2 | 50 | 75 | 152 | 360 | 3.05 |
| 11/4-6 | 31.6 | 32.6 | 46.0 | 48.0 | 49.5 | 52.5 | 41 | 62 | 124 | 460 | 3.95 |
| 11/2-6 | 37.7 | 38.8 | 53.0 | 55.0 | 56.5 | 59.5 | 36 | 54 | 108 | 560 | 4.93 |
| 13/4-6 | 44.7 | 45.8 | 59.8 | 61.8 | 64.5 | 67.5 | 32 | 48 | 96 | 640 | 5.02 |
| 2-6 | 50.5 | 52.0 | 66.2 | 68.2 | 70.5 | 73.5 | 32 | 48 | 96 | 720 | 6.73 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT589

SAE 100R15 Wire Spiral Hydraulic Hose

- Hose Construction

- Inner Tube:black hot oil resistant synthetic rubber

- Reinforcement:four or six plies of spiraled high tensile steel wire

- Outer layer:black oil, weather, and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.Remarkable performance on high pressure,high impulse,and low bend applications.

| SIZE | SIZE | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -6 | 3/8 | 9.5 | 10.5 | 18.6 | 19.8 | 21.0 | 23.0 | 42 | 84 | 168 | 150 | 0.93 |
| -8 | 1/2 | 12.5 | 13.5 | 21.6 | 22.8 | 24.2 | 26.2 | 42 | 84 | 168 | 200 | 1.10 |
| -12 | 3/4 | 18.6 | 19.8 | 27.8 | 29.0 | 30.0 | 32.0 | 42 | 84 | 168 | 265 | 1.54 |
| -16 | 1 | 25.0 | 26.4 | 34.6 | 36.6 | 37.2 | 39.6 | 42 | 84 | 168 | 330 | 2.17 |
| -20 | 11/4 | 31.4 | 33.0 | 46.4 | 48.4 | 48.7 | 51.7 | 42 | 84 | 168 | 445 | 4.08 |
| -24 | 11/2 | 37.7 | 39.3 | 52.0 | 54.0 | 54.5 | 57.5 | 42 | 84 | 168 | 530 | 4.67 |
| -32 | 2 | 50.4 | 52.0 | 66.0 | 68.0 | 68.5 | 71.5 | 42 | 84 | 168 | 680 | 6.71 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.