LTSA599
ISO18752-DC Super Artery Steel Wire Spiral Hose
· Hose Construction
· Inner Tube:CR/NBR synthetic rubber
· Reinforcement:Multi-spiraled high tensile super flexible steel wire,
Four plies ≥ 1 million impulse cycles
· Outer Layer:Skiving-free abrasion and weather resistant synthetic rubber
· Temperature Range:-40°C to +120°C (-40°F  +248°F) -55°C  +100°C (-67°F to +212°F)
· Application:Remarkable performance on tight bend radius, high pressure,long service life, and high impulse,weather resistant for more than five years and warrantied for two years with Letone hose fittings and HNBR seals.Widely apply to excavator and other heavy duty construction machinery or hash working environment.

	SIZE
	I.D
	O.D
	O.D
	MAX.W.P
	P.P
	MIN.B.R

	DASH
	IN
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	

	
	
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	mm

	10-4
	3/8"
	9.5
	10.5
	17.8
	19.0
	20.5
	22.5
	56
	224
	100

	13-4
	1/2"
	12.5
	13.5
	19.8
	21.0
	21.8
	23.8
	42
	168
	140

	16-4
	5/8"
	15.9
	16.6
	23.9
	25.1
	26.0
	28.0
	42
	168
	180

	19-4
	3/4"
	18.8
	19.6
	27.9
	29.1
	30.0
	32.0
	42
	168
	200

	25-4
	1"
	25.0
	25.8
	34.4
	36.4
	36.8
	39.2
	42
	168
	250

	32-4
	1 1/4"
	31.6
	32.6
	40.9
	42.9
	43.3
	45.7
	35
	140
	400

	38-4
	1 1/2"
	37.8
	38.8
	48.1
	50.1
	51.3
	53.7
	32
	128
	480

	51-4
	2"
	50.7
	52
	62.6
	63.8
	65.6
	67.4
	25
	100
	650

	32-6
	1 1/4"
	31.6
	32.6
	46.4
	48.4
	49.0
	51.4
	42
	168
	400

	38-6
	1 1/2"
	37.7
	38.8
	52.0
	54.0
	54.8
	57.0
	42
	168
	480

	51-6
	2"
	50.7
	52
	66.4
	67.6
	69.1
	70.9
	42
	168
	630


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT599
ISO18752-CC Artery Wire Spiral Hydraulic Hose
· Hose Construction
· Inner Tube:NBR synthetic rubber
· Reinforcement:Four or six plies of spiraled high tensile steel wire,tested with 800,000 impulse cycles without leakage
· Outer Layer:Skiving-free abrasion and weather resistant synthetic rubber
· Temperature Range:-40°C to +120°C (-40°F to +248°F) -55°C to +100°C (-67°F to +212°F)
· Application:Remarkable performance on high pressure and high impulse. Widely apply to excavator and other heavy duty construction machinery.
	SIZE
	ImperialStandard
	Metric Specifications
	I.D
	W.D
	O.D
	MAX.W.P
	P.P
	MIN.B.P
	MIN.Impulse
	MIN.B.R
	W.T

	
	SIZE
	SIZE
	MIN
	MAX
	MIN
	MAX
	MIN
	MAX
	
	
	
	10k
	
	

	
	DASH
	IN
	MM
	MM
	MM
	MM
	MM
	MM
	MPA
	MPA
	MPA
	CYCLES
	MM
	Kg/m

	-4
	1/4-4S
	6.2
	6.0
	6.8
	15.0
	16.2
	18.0
	20.0
	69
	138
	276
	50
	120
	0.60

	-6
	3/8-4S
	10
	9.5
	10.5
	17.8
	19.0
	20.5
	22.5
	56
	112
	224
	50
	150
	0.71

	-8
	1/2-4S
	12.5
	12.8
	13.5
	19.8
	21.0
	21.8
	23.8
	42
	84
	168
	80
	190
	0.82

	-10
	5/8-4S
	16
	15.9
	16.6
	23.9
	25.1
	26.0
	28.0
	42
	84
	168
	80
	200
	1.15

	-12
	3/4-4S
	19
	18.8
	19.6
	27.9
	29.1
	30.0
	32.0
	42
	84
	168
	80
	224
	1.56

	-16
	1-4S
	25
	25.0
	25.8
	34.4
	36.4
	36.8
	39.2
	42
	84
	168
	80
	272
	2.13

	-20
	1 1/4-4S
	31.5
	31.6
	32.6
	40.9
	42.9
	43.3
	45.7
	35
	70
	140
	80
	370
	2.56

	-24
	1 1/2-4S
	38
	37.8
	38.8
	48.1
	50.1
	51.3
	53.7
	32
	64
	128
	80
	540
	3.18

	-32
	2-4S
	51
	50.7
	52
	62.6
	63.8
	65.6
	67.4
	25
	50
	100
	80
	660
	4.46

	-20
	1 1/4-6S
	31.5
	31.6
	32.6
	46.0
	48.0
	48.8
	51.2
	42
	84
	168
	80
	420
	4.07

	-24
	1 1/2-6S
	38
	37.7
	38.8
	52.0
	54.0
	54.8
	57.2
	42
	84
	168
	80
	500
	4.63

	-32
	2-6S
	51.5
	51.6
	51.8
	66.4
	67.6
	69.1
	70.9
	42
	84
	168
	80
	650
	6.32


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT588
EN 856-4SH | MSHA | MA Wire Spiral Hydraulic Hose
· Hose Construction
· Inner Tube:Black oil resistant synthetic rubber
· Reinforcement:Four plies of spiraled high tensile steel wire
· Outer Layer:Black oil and weather resistant synthetic rubber
· Temperature Range:-40°C to +100°C (-40°F  +212°F)
· Application:Suitable for conveying water-based,petroleum-based, and biodegradable hydraulic oil.
	Specification
	Specification
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	SIZE
	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-10
	5/8
	15.5
	16.7
	23.9
	25.1
	26.0
	28.0
	45
	90
	180
	250
	1.15

	-12
	3/4
	18.6
	19.8
	27.6
	29.2
	30.0
	32.0
	42
	84
	168
	280
	1.54

	-16
	1
	25.0
	26.4
	34.4
	36.0
	37.0
	39.0
	38
	76
	152
	340
	2.02

	-20
	1 1/4
	31.4
	33.0
	40.9
	42.9
	43.8
	46.2
	32.5
	65
	130
	460
	2.48

	-24
	1 1/2
	37.7
	39.3
	48.1
	50.1
	51.3
	53.7
	29
	58
	116
	560
	3.18

	-32
	2
	50.4
	52.0
	62.2
	64.2
	65.3
	67.7
	25
	50
	100
	700
	4.46


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT583
EN856-4SP|MSHA Wire Spiral Hydraulic Hose
· Hose Construction
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:four plies of spiraled high tensile steel wire
· Outer Layer:black oil and weather resistant synthetic rubber
· Temperature Range:-40°C  +100°C (-40°F  +212°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.
	 SIZE
	 SIZE
	 I.D
	W.D
	0.D
	Max.W.P
	 P.P
	Min.B.P
	Min.B.R
	 W.T

	
	
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-4
	1/4
	6.2
	7.0
	14.3
	15.5
	16.6
	18.6
	45
	90
	180
	150
	0.60

	-6
	3/8
	9.5
	10.5
	16.9
	18.1
	19.1
	21.1
	44.5
	89
	178
	180
	0.71

	-8
	1/2
	12.5
	13.5
	19.8
	21.0
	21.8
	23.8
	41.5
	83
	166
	230
	0.82

	-10
	5/8
	15.5
	16.7
	23.0
	24.6
	25.4
	27.4
	35
	70
	140
	250
	1.01

	-12
	3/4
	18.6
	19.8
	27.4
	29.0
	30.0
	32.0
	35
	70
	140
	300
	1.43

	-16
	1
	25.0
	26.4
	34.5
	36.1
	37.0
	39.0
	32
	64
	128
	340
	1.97

	-20
	11/4
	31.4
	33.0
	45.0
	46.4
	47.4
	49.8
	21
	42
	84
	460
	2.96

	-24
	11/2
	37.7
	39.3
	50.9
	52.3
	53.8
	56.2
	18.5
	37
	74
	560
	3.42

	-32
	2
	50.4
	52.0
	64.3
	66.3
	66.9
	69.3
	16.5
	33
	66
	660
	4.77


LT581
SAE 100R12|MSHA Wire Spiral Hydraulic Hose
· Hose Construction
· Inner Tube:black hot oil resistant synthetic rubber
· Reinforcement:four plies of spiraled high tensile steel wire
· Outer Layer:black oil and weather resistant synthetic rubber
· Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil under harsh working conditions.
	 SIZE
	 SIZE
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	
	
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-6
	3/8
	9.5
	10.5
	16.9
	18.1
	19.0
	21.0
	28
	56
	112
	125
	0.71

	-8
	1/2
	12.5
	13.5
	20.1
	21.3
	22.1
	24.1
	28
	56
	112
	180
	0.85

	-10
	5/8
	15.5
	16.7
	24.0
	25.2
	26.5
	28.5
	28
	56
	112
	200
	1.06

	-12
	3/4
	18.6
	19.8
	26.9
	28.4
	29.1
	31.1
	28
	56
	112
	240
	1.33

	-16
	1
	25.0
	26.4
	34.2
	35.8
	36.3
	38.7
	28
	56
	112
	300
	1.83

	-20
	11/4
	31.4
	33.0
	42.9
	44.9
	45.3
	47.7
	21
	42
	84
	420
	2.67

	-24
	11/2
	37.7
	39.3
	49.4
	51.4
	52.3
	54.7
	17.5
	35
	70
	500
	3.12

	-32
	2
	50.8
	52.0
	62.5
	64.8
	65.1
	68.3
	17.5
	35
	70
	640
	4.48


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT582
SAE 100R13|MSHA Wire Spiral Hydraulic Hose
· Hose Construction
· Inner Tube:black hot oil resistant synthetic rubber
· Reinforcement:four or six plies of spiraled high tensile steel wire
· Outer Layer:black oil and weather resistant synthetic rubber
· Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil under harsh working conditions.
	 SIZE
	 SIZE
	  I.D
	 W.D
	 O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	
	
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-12
	3/4
	18.6
	19.8
	28.2
	29.4
	31.2
	33.2
	35
	70
	140
	240
	1.61

	-16
	1
	25.0
	26.4
	34.8
	36.4
	37.3
	39.7
	35
	70
	140
	300
	2.06

	-20
	11/4
	31.4
	31.4
	46.0
	48.0
	48.8
	51.2
	35
	70
	140
	420
	3.84

	-24
	11/2
	37.7
	37.7
	53.0
	55.0
	55.8
	58.2
	35
	70
	140
	500
	4.60

	-32
	2
	50.4
	50.4
	67.1
	69.1
	69.5
	72.5
	35
	70
	140
	640
	6.61


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT585
MT/T98|MSHA Wire Spiral Hydraulic Hose For Mining
· Hose Construction:
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:four or six plies of spiraled high tensile steel wire
· Outer Layer:black oil,weather, and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable for conveying medium like mineral oil,water-based hydraulic oil,or water in coal mining machinery such as coal mining hydraulic supportand coal shearer.
	Specification
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	 SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	3/8-4
	9.5
	10.5
	18.2
	19.8
	22.4
	24.4
	70
	105
	210
	180
	0.90

	1/2-4
	12.5
	13.5
	21.4
	23.0
	25.2
	27.2
	57
	86
	172
	210
	1.05

	5/8-4
	15.7
	16.6
	25.2
	26.8
	29.0
	31.0
	53
	80
	160
	260
	1.40

	3/4-4
	18.7
	19.8
	29.2
	30.4
	33.0
	35.0
	46
	69
	140
	280
	1.75

	7/8-4
	21.7
	22.8
	31.7
	32.9
	36.0
	38.0
	41
	62
	124
	320
	1.93

	1-4
	24.7
	25.8
	35.2
	36.4
	38.8
	41.2
	35
	53
	112
	360
	2.14

	11/4-4
	31.6
	32.6
	43.2
	44.6
	46.8
	49.2
	32
	48
	84
	460
	2.82

	11/2-4
	37.7
	38.8
	49.8
	51.8
	54.3
	56.7
	25
	38
	75
	560
	3.41

	13/4-4
	44.7
	45.8
	56.8
	58.8
	61.5
	64.5
	21
	32
	64
	640
	4.03

	2-4
	50.5
	52.0
	62.8
	64.8
	65.0
	67.4
	21
	32
	64
	720
	4.43

	3/8-6
	9.5
	10.5
	20.0
	22.0
	24.0
	26.0
	80
	120
	240
	180
	1.20

	1/2-6
	12.5
	13.5
	23.4
	24.6
	26.5
	28.5
	72
	108
	216
	210
	1.40

	5/8-6
	15.7
	16.6
	28.0
	30.0
	31.5
	34.5
	70
	105
	204
	260
	2.10

	3/4-6
	18.7
	19.8
	32.0
	34.0
	35.5
	37.5
	60
	90
	180
	280
	2.47

	7/8-6
	21.7
	22.8
	35.0
	37.0
	39.5
	42.5
	53
	80
	160
	320
	2.80

	1-6
	24.7
	25.8
	38.0
	39.6
	41.8
	44.2
	50
	75
	152
	360
	3.05

	11/4-6
	31.6
	32.6
	46.0
	48.0
	49.5
	52.5
	41
	62
	124
	460
	3.95

	11/2-6
	37.7
	38.8
	53.0
	55.0
	56.5
	59.5
	36
	54
	108
	560
	4.93

	13/4-6
	44.7
	45.8
	59.8
	61.8
	64.5
	67.5
	32
	48
	96
	640
	5.02

	2-6
	50.5
	52.0
	66.2
	68.2
	70.5
	73.5
	32
	48
	96
	720
	6.73


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT589
SAE 100R15 Wire Spiral Hydraulic Hose
· Hose Construction
· Inner Tube:black hot oil resistant synthetic rubber
· Reinforcement:four or six plies of spiraled high tensile steel wire
· Outer layer:black oil, weather, and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.Remarkable performance on high pressure,high impulse,and low bend applications.
	 SIZE
	  SIZE
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	
	
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-6
	3/8
	9.5
	10.5
	18.6
	19.8
	21.0
	23.0
	42
	84
	168
	150
	0.93

	-8
	1/2
	12.5
	13.5
	21.6
	22.8
	24.2
	26.2
	42
	84
	168
	200
	1.10

	-12
	3/4
	18.6
	19.8
	27.8
	29.0
	30.0
	32.0
	42
	[bookmark: _GoBack]84
	168
	265
	1.54

	-16
	1
	25.0
	26.4
	34.6
	36.6
	37.2
	39.6
	42
	84
	168
	330
	2.17

	-20
	11/4
	31.4
	33.0
	46.4
	48.4
	48.7
	51.7
	42
	84
	168
	445
	4.08

	-24
	11/2
	37.7
	39.3
	52.0
	54.0
	54.5
	57.5
	42
	84
	168
	530
	4.67

	-32
	2
	50.4
	52.0
	66.0
	68.0
	68.5
	71.5
	42
	84
	168
	680
	6.71


The items marked with * are for reference only; the actual specifications are subject to the hose body.
