LT681
SAE 100RAT|EN853 SN|DNV Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:black oil,weather,and abrasion resistant synthetic rubber
· Temperature Range:-40°C  +100°C (-40°F  +212°F)
· [bookmark: _GoBack]Application:Suitable for conveying water-based,petroleum-based,and  biodegradable hydraulic oil.
	Specification
	I.D
	W.D
	O.D.
	Max.W.P
	P.P
	Min.B.P.  
	Min.B.R.  
	W.T

	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	Max.W.P
	
	
	
	

	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	3/16-1
	4.6
	5.4
	9.0
	10.0
	11.0
	12.2
	25.0
	50.0
	100.0
	90
	0.17

	1/4-1
	6.2
	7.0
	10.6
	11.6
	12.8
	14.0
	22.5
	45.0
	90.0
	100
	0.22

	5/16-1
	7.7
	8.5
	12.5
	13.5
	14.6
	15.8
	21.5
	43.0
	85.0
	115
	0.28

	3/8-1
	9.3
	10.3
	14.5
	15.7
	16.8
	18.0
	18.0
	36.0
	72.0
	130
	0.34

	1/2-1
	12.3
	13.5
	17.5
	19.0
	20.1
	21.3
	16.0
	32.0
	64.0
	180
	0.42

	5/8-1
	15.5
	16.7
	20.6
	22.2
	23.2
	24.8
	13.0
	26.0
	52.0
	200
	0.51

	3/4-1
	18.6
	19.8
	24.3
	25.5
	27.0
	29.0
	10.5
	21.0
	42.0
	240
	0.68

	1-1
	25.0
	26.4
	31.9
	33.1
	35.2
	36.8
	8.8
	17.5
	35.0
	300
	0.96

	1 1/4-1
	31.4
	33.0
	39.2
	40.8
	42.3
	44.7
	6.3
	13.0
	25.0
	420
	1.19

	1 1/2-1
	37.7
	39.3
	44.9
	46.5
	48.0
	50.4
	5.0
	10.0
	20.0
	500
	1.34

	2-1
	50.4
	52.0
	58.7
	60.3
	61.8
	64.2
	4.0
	8.0
	16.0
	630
	1.89

	3/16-2
	4.6
	5.4
	10.6
	11.6
	12.7
	13.9
	41.5
	83.0
	166.0
	90
	0.27

	1/4-2
	6.1
	7.0
	12.6
	13.6
	14.4
	15.6
	40.0
	80.0
	160.0
	100
	0.35

	5/16-2
	7.7
	8.5
	14.1
	15.1
	15.7
	16.9
	35.0
	70.0
	140.0
	115
	0.40

	3/8-2
	9.3
	10.3
	16.3
	17.5
	18.1
	19.3
	33.0
	66.0
	132.0
	130
	0.51

	1/2-2
	12.3
	13.5
	19.4
	20.6
	21.6
	22.8
	27.5
	55.0
	110.0
	180
	0.63

	5/8-2
	15.5
	16.7
	22.2
	23.8
	24.6
	26.2
	25.0
	50.0
	100.0
	200
	0.74

	3/4-2
	18.6
	19.8
	26.2
	27.8
	28.8
	30.4
	21.5
	43.0
	86.0
	240
	0.92

	1-2
	25.0
	26.4
	33.6
	34.8
	36.3
	37.9
	16.5
	32.5
	66.0
	300
	1.33

	1 1/4-2
	31.4
	33.0
	43.6
	45.0
	46.3
	48.7
	12.5
	25.0
	50.0
	420
	1.97

	1 1/2-2
	37.7
	39.3
	49.6
	51.4
	52.8
	55.2
	9.0
	18.0
	36.0
	500
	2.33

	2-2
	50.4
	52.0
	62.3
	64.7
	65.6
	68.0
	8.0
	16.0
	32.0
	630
	2.88


LT682
EN853 ST Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:black oil,weather,and abrasion resistant synthetic rubber
· Temperature Range:-40°C to +100°C (-40°F to +212°F)
· Application:Suitable for conveying water-based,petroleum-based, and biodegradable hydraulic oil.
	Specification
	I.D
	W.D
	O.D.
	MaxW.P
	P.P
	Min.B.P.  
	Min.B.R.  
	W.T

	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	3/16-1
	4.6
	5.4
	9.0
	10.0
	11.5
	12.9
	25.0
	50.5
	100.0
	90
	0.18

	1/4-1
	6.2
	7.0
	10.6
	11.6
	14.6
	16.0
	22.5
	45.0
	90.0
	100
	0.27

	5/16-1
	7.7
	8.5
	12.5
	13.5
	16.2
	17.6
	21.5
	43.0
	85.0
	115
	0.33

	3/8-1
	9.3
	10.3
	14.5
	15.7
	18.5
	19.9
	18.0
	36.0
	72.0
	130
	0.40

	1/2-1
	12.3
	13.5
	17.5
	19.0
	21.8
	23.4
	16.0
	32.0
	64.0
	180
	0.50

	5/8-1
	15.5
	16.7
	20.6
	22.2
	24.7
	26.3
	13.0
	26.0
	52.0
	200
	0.58

	3/4-1
	18.6
	19.8
	24.3
	25.5
	28.7
	30.3
	10.5
	21.0
	42.0
	240
	0.73

	1-1
	25.0
	26.4
	31.9
	33.1
	36.3
	37.9
	8.8
	17.5
	35.0
	300
	1.04

	1 1/4-1
	31.4
	33.0
	39.2
	40.8
	43.3
	45.7
	6.3
	15.0
	25.0
	420
	1.28

	1 1/2-1
	37.7
	39.3
	44.9
	46.5
	49.8
	52.2
	5.0
	10.0
	20.0
	500
	1.51

	2-1
	50.4
	52.0
	58.7
	60.3
	64.3
	66.7
	4.0
	8.0
	16.0
	630
	2.20

	3/16-2
	4.6
	5.4
	10.6
	11.6
	14.6
	16.0
	41.5
	83.0
	165.0
	90
	0.33

	1/4-2
	6.1
	7.0
	12.6
	13.6
	16.3
	17.7
	40.0
	80.0
	160.0
	100
	0.42

	5/16-2
	7.7
	8.5
	14.1
	15.1
	18
	19.4
	35.0
	70.0
	140.0
	115
	0.47

	3/8-2
	9.3
	10.3
	16.3
	17.5
	20.3
	21.7
	33.0
	66.0
	132.0
	130
	0.60

	1/2-2
	12.3
	13.5
	19.4
	20.6
	23.4
	25.0
	27.5
	55.0
	110.0
	180
	0.73

	5/8-2
	15.5
	16.7
	22.2
	23.8
	26.6
	28.2
	25.0
	50.0
	100.0
	200
	0.85

	3/4-2
	18.6
	19.8
	26.2
	27.8
	30.6
	32.2
	21.5
	43.0
	85.0
	240
	1.03

	1-2
	25.0
	26.4
	33.6
	34.8
	37.7
	39.3
	16.5
	32.5
	65.0
	300
	1.44

	1 1/4-2
	31.4
	33.0
	43.6
	45.0
	48.0
	50.4
	12.5
	25.0
	50.0
	420
	2.14

	1 1/2-2
	37.7
	39.3
	49.6
	51.4
	54.4
	56.8
	9.0
	18.0
	36.0
	500
	2.50

	2-2
	50.4
	52.0
	62.3
	64.7
	67.0
	69.4
	8.0
	16.0
	32.0
	630
	3.07


LT699
ISO 18752-AC/BC Artery Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:NBR synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire,one braid≥300,000 impulse cycles,two braids≥500,000 impulse cycles
· Outer Layer:skiving-free oil,abrasion,and weather resistant synthetic rubber
· Temperature Range:-40℃~+100℃(-40°F~+212°F);-55℃~+100℃(-67°F~+212°F)
· Application:Remarkable performance on high pressure and high impulse.Widely apply to excavator and other heavy duty construction machinery.
	SIZE
	Specification
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.Impulse
	Min.B.R
	W.T

	
	
	
	
	
	
	
	
	10K
	
	

	
	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	
	

	
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	CYCLES
	mm
	kg/m

	-4
	1/4-1
	5.8
	6.5
	10.7
	11.7
	12.9
	13.9
	25
	50
	100
	30
	80
	0.20

	-5
	5/16-1
	7.7
	8.5
	12.5
	13.5
	14.7
	15.7
	25
	50
	100
	30
	92
	0.25

	-6
	3/8-1
	9.8
	10.5
	14.5
	15.5
	16.9
	17.9
	21
	42
	84
	30
	104
	0.32

	-8
	1/2-1
	12.8
	13.5
	17.7
	18.7
	20.2
	21.2
	18
	36
	72
	30
	144
	0.40

	-10
	5/8-1
	15.8
	16.6
	20.7
	21.7
	23.5
	24.5
	14
	28
	56
	30
	160
	0.50

	-12
	3/4-1
	18.8
	19.8
	24.4
	25.4
	27.0
	29.0
	14
	28
	56
	30
	192
	0.67

	-16
	1-1
	24.8
	25.8
	32
	33
	35.4
	36.6
	9
	18
	36
	30
	240
	0.91

	-20
	11/4-1
	31.4
	33
	39.3
	40.7
	42.7
	44.3
	6.3
	13
	25
	30
	400
	1.19

	-24
	11/2-1
	37.7
	39.3
	45
	46.4
	48.4
	50
	5
	10
	20
	30
	480
	1.33

	-32
	2-1
	50.4
	52
	58.8
	60.2
	62.2
	63.8
	4
	8
	16
	30
	560
	1.87

	-4
	1/4-2
	5.8
	6.5
	12.6
	13.6
	14.5
	15.5
	42
	84
	168
	50
	80
	0.35

	-5
	5/16-2
	7.7
	8.5
	14
	15
	15.8
	16.8
	35
	84
	140
	50
	92
	0.40

	-6
	3/8-2
	9.8
	10.5
	16.4
	17.4
	18.2
	19.2
	35
	70
	140
	50
	104
	0.52

	-8
	1/2-2
	12.8
	13.5
	19.5
	20.5
	21.7
	22.7
	28
	56
	112
	50
	144
	0.63

	-10
	5/8-2
	15.8
	16.6
	22.5
	23.5
	24.9
	25.9
	28
	56
	112
	50
	160
	0.76

	-12
	3/4-2
	18.8
	19.8
	26.5
	27.5
	29
	30.2
	25
	50
	100
	50
	192
	0.94

	-16
	1-2
	24.8
	25.8
	33.5
	34.5
	36.5
	37.7
	21
	42
	84
	50
	240
	1.37

	-20
	11/4-2
	31.4
	33.0
	43.5
	44.9
	46.7
	48.3
	14
	28
	56
	50
	400
	2.00

	-24
	11/2-2
	37.7
	39.3
	49.8
	51.2
	53.2
	54.8
	9.0
	18
	36
	50
	480
	2.30

	-32
	2-2
	50.4
	52.0
	62.5
	63.9
	66
	67.6
	8.0
	16
	32
	50
	610
	3.02


LT683
EN857 SC Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:Black oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:black oil, weather, and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil
	Specification
	I.D
	W.D
	O.D.
	Max.W.P
	P.P
	Min.B.P.  
	Min.B.R.  
	W.T

	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	psi
	MPa
	psi
	MPa
	psi
	inch
	mm
	kg/m

	1/4-1
	6.1
	6.9
	9.9
	10.9
	11.8
	13.2
	22.5
	3260
	45.0
	6265
	90.0
	13050
	2.95
	75
	0.18

	5/16-1
	7.7
	8.5
	11.2
	12.2
	13.1
	14.5
	21.5
	3120
	43.0
	6235
	86.0
	12470
	3.35
	85
	0.20

	3/8-1
	9.3
	10.1
	13.3
	14.3
	15.1
	16.5
	18.0
	2610
	36.0
	5220
	72.0
	10440
	3.54
	90
	0.27

	1/2-1
	12.3
	13.5
	16.4
	17.6
	18.9
	20.3
	16.0
	2320
	32.0
	4640
	64.0
	9280
	5.12
	130
	0.35

	5/8-1
	15.5
	16.7
	19.8
	21.0
	21.9
	23.3
	13.0
	1885
	26.0
	3770
	52.0
	7540
	5.91
	150
	0.42

	3/4-1
	18.6
	19.8
	23.1
	24.5
	25.6
	27.2
	10.5
	1520
	21.0
	3045
	42.0
	6090
	7.09
	180
	0.54

	1-1
	25.0
	26.4
	30.5
	31.9
	33.2
	34.8
	8.8
	1280
	17.6
	2550
	35.5
	5100
	9.06
	230
	0.78

	1/4-2
	6.1
	6.9
	11.2
	12.2
	12.9
	14.3
	40.0
	5800
	80
	11600
	160.0
	23200
	2.96
	75
	0.28

	5/16-2
	7.7
	8.5
	12.8
	13.8
	14.5
	15.9
	35.0
	5075
	70
	10150
	140.0
	20300
	3.35
	85
	0.32

	3/8-2
	9.3
	10.1
	14.9
	15.9
	16.8
	18.2
	33
	4785
	66
	9570
	132.0
	19140
	3.54
	90
	0.43

	1/2-2
	12.3
	13.5
	18.0
	19.2
	20.0
	21.6
	27.5
	3990
	55
	7975
	110.0
	15950
	5.12
	130
	0.52

	5/8-2
	15.5
	16.7
	21.4
	22.6
	23.2
	24.8
	25
	3625
	50
	7150
	100.0
	14500
	6.69
	170
	0.66

	3/4-2
	18.6
	19.8
	25.0
	26.4
	27.4
	29.0
	21.5
	3120
	43
	6235
	86.0
	12470
	7.87
	200
	0.83

	1-2
	25.0
	26.4
	32.4
	33.8
	34.5
	36.1
	16.5
	2390
	33
	4785
	66.0
	9570
	9.84
	250
	1.17


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT685
MT/T98 Wire Braid Hydraulic Hose For Mining
· Hose Construction
· Inner Layer:black oil resistant synthetic rubber
· Reinforcement:one, two, or three braids of high tensile super flexible steel wire
· Outer Layer:black oil, weather,and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable for conveying medium like mineral oil,water-based hydraulic oil,orwater in coalmining machinery such as coal mining hydraulic  supportand coal shearer
	SIZE
	I.D 
mm
	W.D
mm
	O.D 
mm
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	IN
	Min
	Max
	Min
	Max
	Min
	Max
	MPa
	MPa
	MPa
	mm
	kg/m

	1/4-1
	6.1
	6.9
	11.1
	12.1
	14.2
	15.4
	32
	40
	80
	100
	0.26

	5/16-1
	7.8
	8.5
	13.0
	14.0
	16.2
	17.4
	28
	35
	70
	115
	0.31

	3/8-1
	9.8
	10.5
	15.1
	16.1
	18.1
	19.3
	25.6
	32
	64
	130
	0.37

	1:/2-1
	12.8
	13.5
	18.9
	19.9
	21.9
	23.1
	22.4
	33.6
	56
	180
	0.48

	5/8-1
	15.8
	16.6
	22.0
	23.0
	24.7
	26.3
	16.8
	21
	42
	205
	0.57

	3//4-1
	18.8
	19.8
	25.0
	26.0
	27.6
	29.2
	14.4
	18
	36
	240
	0.66

	7/8-1
	21.8
	22.8
	28.0
	29.0
	30.6
	32.2
	12.8
	16
	32
	280
	0.73

	1-1
	25.0
	26.0
	31.3
	32.5
	34.2
	35.8
	11.2
	14
	28
	300
	0.86

	11/4-1
	31.6
	33.6
	38.3
	39.9
	41.8
	44.2
	9.0
	11.5
	22.5
	420
	1.15

	11/2-1
	37.7
	39.8
	44.8
	46.4
	48.1
	50.3
	7.0
	9
	17.5
	500
	1.29

	13/4-1
	44.6
	45.6
	51.8
	53.4
	55.4
	57.6
	5.0
	8
	12.5
	550
	1.55

	2-1
	50.7
	52.0
	57.8
	59.4
	61.3
	63.7
	3.0
	6
	7.5
	630
	1.77

	1/4-2
	6.1
	6.9
	12.9
	13.9
	16.0
	17.2
	60.0
	75
	150
	100
	0.40

	5/16-2
	7.8
	8.5
	14.9
	15.9
	18.0
	19.2
	48.0
	60
	120
	115
	0.47

	3/8-2
	9.8
	10.5
	16.6
	17.6
	19.9
	21.1
	40.0
	50
	100
	130
	0.55

	1/2-2
	12.8
	13.5
	20.7
	21.7
	23.7
	24.9
	36.0
	45
	90
	180
	0.71

	5/8-2
	15.8
	16.6
	23.4
	24.6
	26.5
	28.1
	32.0
	40
	80
	205
	0.86

	3/4-2
	18.8
	19.8
	26.4
	27.6
	29.4
	31
	25.0
	31.5
	62.5
	240
	0.95

	7/8-2
	21.8
	22.8
	29.5
	30.7
	32.3
	34.1
	22.0
	27.5
	55
	280
	1.05

	1-2
	25.0
	26.0
	32.8
	34.0
	36
	37.6
	21.0
	26.5
	52.5
	300
	1.25

	11/4-2
	31.6
	33.6
	39.8
	41.4
	43.6
	45.8
	17.0
	21.5
	42.5
	420
	1.57

	11/2-2
	37.7
	39.8
	46.4
	48.0
	49.8
	52.2
	12.0
	15
	30
	500
	1.88

	13/4-2
	44.6
	45.6
	53.4
	55.0
	56.8
	59.2
	9.0
	13.5
	22.5
	55
	2.13

	2-2
	50.7
	52.0
	59.4
	61.0
	62.8
	65.2
	8.0
	12
	20
	630
	2.45

	5/16-3
	7.8
	8.5
	16.5
	17.5
	19.6
	20.8
	50.0
	75
	125
	115
	0.61

	3/8-3
	9.8
	10.5
	18.0
	19.2
	21.5
	22.7
	45.0
	62.5
	112.5
	130
	0.69

	1/2-3
	12.8
	13.5
	22.1
	23.3
	25.5
	26.7
	40.0
	56
	100
	180
	0.94

	5/8-3
	15.8
	16.6
	25.1
	26.3
	28.3
	29.9
	35.0
	43.5
	87.5
	205
	1.16

	3/4-3
	18.8
	19.8
	28.1
	29.3
	31.2
	32.8
	28.0
	35
	70.5
	240
	1.26

	7/8-3
	21.8
	22.8
	31.1
	32.3
	34.2
	35.8
	25.0
	31.5
	62.5
	280
	1.43

	1-3
	25.0
	26.0
	34.6
	35.6
	37.2
	38.8
	24.0
	30
	60.5
	300
	1.59

	11/4-3
	31.6
	33.6
	41.4
	43.0
	45.4
	47.6
	19.0
	24
	47.5
	420
	2.05

	11/2-3
	37.7
	39.8
	48.0
	49
	51.8
	54.2
	15.0
	19
	37.5
	500
	2.44


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT686
MT/T98 Wire Braid Hydraulic Hose For Mining
· Hose Construction
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:oil,weather,and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable for conveying medium like mineral oil,water-based hydraulic oil,or water in coal mining machinery such as coal mining hydraulic support and coal shearer.
	Specification
	Specification
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	SIZE
	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	64
	2 1/2-1
	63.5
	65.3
	71
	73
	76
	80
	3.5
	5.25
	10.5
	800
	2.42

	76
	3-1
	75.5
	77.5
	83
	85
	88
	92
	3
	4.5
	9
	920
	2.86

	85
	3 3/8-1
	84.5
	86.7
	92
	94
	97
	101
	2.5
	3.75
	7.5
	1000
	3.10

	89
	3 1/2-1
	88.4
	90
	96.5
	98.5
	102
	106
	2.5
	3.75
	7.5
	1100
	3.34

	102
	4-1
	101
	104.5
	110
	115
	116
	121
	2
	3
	6
	1300
	3.78

	64
	2 1/2-2
	63.5
	65.3
	73
	75
	78
	80
	7
	10.5
	21
	800
	3.30

	76
	3-2
	75.5
	77.5
	85
	87
	90
	94
	6
	9
	18
	920
	3.90

	85
	3 3/8-2
	84.5
	86.7
	94
	96
	99
	103
	5
	7.5
	15
	1000
	4.30

	89
	3 1/2-2
	88.4
	90
	98.5
	100.5
	104
	108
	5
	7.5
	15
	1100
	4.54

	102
	4-2
	101
	104.5
	112
	116
	118
	123
	4
	6
	12
	1300
	5.50


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT687
SAE 100R16 Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:black hot oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:black oil,weather,and abrasion resistant synthetic rubber
· Temperature Range:-40℃~+100℃(-40°F~+212°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.
	Specification
	Specification
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	SIZE
	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	psi
	MPa
	psi
	MPa
	psi
	mm
	kg/m

	-4
	1/4
	6.2
	7.0
	10.7
	11.7
	12.6
	13.8
	40
	5800
	80
	11600
	160
	23200
	50
	0.3

	-5
	5/16
	7.7
	8.5
	12.1
	13.3
	14.4
	15.6
	35
	5075
	70
	10150
	140
	20300
	55
	0.34

	-6
	3/8
	9.3
	10.1
	14.5
	15.5
	16.4
	17.6
	33
	4785
	66
	9570
	132
	19140
	65
	0.42

	-8
	1/2
	12.3
	13.5
	17.9
	18.9
	19.9
	21.1
	27.5
	3990
	55
	7975
	110
	15950
	90
	0.54

	-10
	5/8
	15.5
	16.7
	21.4
	22.6
	23.2
	24.8
	25
	3625
	50
	7150
	100
	14500
	100
	0.68

	-12
	3/4
	18.6
	19.8
	25.1
	26.3
	27.2
	28.8
	21.5
	3120
	43
	6235
	86
	12470
	120
	0.80

	-16
	1
	25.0
	26.4
	32.3
	33.9
	34.1
	36.5
	16.5
	2390
	33
	4785
	66
	9570
	150
	1.15

	-20
	1 1/4
	31.4
	33.0
	40.3
	41.9
	42.8
	45.2
	12.5
	1813
	25
	3625
	50
	7150
	210
	1.83


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT688
SAE 100R17 Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:black oil,weather,and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.
	Specification
	Specification
	I.D
	W.D
	O.D.
	Max.W.P
	P.P
	Min.B.P.  
	Min.B.R.  
	W.T

	SIZE
	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-4
	1/4
	6.2
	7.0
	10.3
	11.3
	12.2
	13.4
	21
	42
	84
	50
	0.19

	-5
	5/16
	7.7
	8.5
	11.8
	12.8
	13.7
	14.9
	21
	42
	84
	55
	0.22

	-6
	3/8
	9.3
	10.1
	13.6
	14.6
	15.5
	16.7
	21
	42
	84
	65
	0.28

	-8
	1/2
	12.3
	13.5
	16.8
	17.8
	19.4
	20.6
	21
	42
	84
	90
	0.38

	-10
	5/8
	15.5
	16.7
	22.2
	23.2
	23.9
	25.1
	21
	42
	84
	100
	0.68

	-12
	3/4
	18.6
	19.8
	25.1
	26.3
	26.9
	28.5
	21
	42
	84
	120
	0.83

	-16
	1
	25.5
	26.4
	33.2
	34.4
	35.7
	37.3
	21
	42
	84
	150
	1.29


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LT689
SAE 100R19 Compact Wire Braid Hydraulic Hose
· Hose Construction
· Inner Tube:black oil resistant synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire
· Outer Layer:black oil,weather,and abrasion resistant synthetic rubber
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.
	Specification
	Specification
	I.D
	W.D
	O.D
	Max.W.P
	P.P
	Min.B.P
	Min.B.R
	W.T

	SIZE
	SIZE
	Min
	Max
	Min
	Max
	Min
	Max
	
	
	
	
	

	DASH
	IN
	mm
	mm
	mm
	mm
	mm
	mm
	MPa
	MPa
	MPa
	mm
	kg/m

	-3
	3/16
	4.6
	5.4
	10.3
	11.9
	11.5
	12.7
	28
	56
	112
	45
	0.237

	-4
	1/4
	6.2
	7.0
	11.1
	12.1
	13.0
	14.4
	28
	56
	112
	50
	0.267

	-5
	5/16
	7.7
	8.5
	12.7
	13.7
	14.6
	16.0
	28
	56
	112
	55
	0.321

	-6
	3/8
	9.3
	10.1
	14.6
	15.6
	16.4
	18.0
	28
	56
	112
	65
	0.359

	-8
	1/2
	12.3
	13.5
	18.0
	19.0
	19.3
	21.3
	28
	56
	112
	90
	0.492

	-10
	5/8
	15.5
	16.7
	20.9
	21.9
	22.5
	24.5
	28
	56
	112
	100
	0.633

	-12
	3/4
	18.6
	19.8
	24.9
	25.9
	26.3
	28.7
	28
	56
	112
	120
	0.764

	-16
	1
	25.0
	26.4
	31.4
	33.0
	33.2
	35.5
	28
	56
	112
	150
	1011


The items marked with * are for reference only; the actual specifications are subject to the hose body.
LTSA699
Exceeds ISO18752-BC Super Artery Wire Braid Hydraulic Hose
· Hose Construction
· Inner Layer:CR/NBR synthetic rubber
· Reinforcement:one or two braids of high tensile super flexible steel wire,
one braid≥300,000 impulse cycles,two braids≥500,000 impulse cycles
· Outer Layer:skiving-free oil,abrasion,and weather resistant synthetic rubber
· Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F); -55°C ~ +100°C (-67°F ~ +212°F)
· Application:Remarkable performance on tight bend radius,high pressure,long service life,and high impulse,weather resistant for more than five years and warrantied for two years with Letone hose fittings and HNBR seals.Widely apply to excavator and other heavy duty construction machinery orhash working environment.
	TYPE
	SIZE(inch)
	I.D.(mm)
	W.P.(MPa)
	B.P.(MPa)
	MIN.B.R.(mm)

	SA699-1BC/CS
	1/4"
	6.4
	29.5
	118
	40

	SA699-1BC/CS
	5/16"
	7.9
	25
	100
	55

	SA699-1BC/CS
	3/8"
	9.5
	23
	92
	65

	SA699-1BC/CS
	1/2"
	12.7
	20
	80
	80

	SA699-1BC/CS
	5/8"
	15.9
	15
	60
	105

	SA699-1BC/CS
	3/4"
	19
	14
	56
	120

	SA699-1BC/CS
	1"
	25.4
	11
	44
	160

	SA699-1BC/CS
	11/4"
	31.8
	10
	40
	300

	SA699-1BC/CS
	11/2"
	38.1
	5
	20
	480

	SA699-1BC/CS
	2"
	50.8
	4
	16
	560

	SA699-2BC/CS
	1/4"
	6.4
	42
	168
	55

	SA699-2BC/CS
	5/16"
	7.9
	38
	152
	60

	SA699-2BC/CS
	3/8"
	9.5
	35
	140
	70

	SA699-2BC/CS
	1/2"
	12.7
	31
	124
	110

	SA699-2BC/CS
	5/8"
	15.9
	28
	112
	130

	SA699-2BC/CS
	3/4"
	19
	25
	100
	160

	SA699-2BC/CS
	1"
	25.4
	21
	84
	210

	SA699-2BC/CS
	11/4"
	31.8
	16.5
	66
	250

	SA699-2BC/CS
	11/2"
	38.1
	13.5
	54
	300

	SA699-2BC/CS
	2"
	50.8
	8
	32
	610


The items marked with * are for reference only; the actual specifications are subject to the hose body.

