LT681

SAE 100RAT|EN853 SN|DNV Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C  +100°C (-40°F  +212°F)

- Application:Suitable for conveying water-based,petroleum-based,and  biodegradable hydraulic oil.

| Specification | I.D |  | W.D |  | O.D. |  | Max.W.P | P.P | Min.B.P. | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | Min | Max | Min | Max | Min | Max | Max.W.P |  |  |  |  |
| IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| 3/16-1 | 4.6 | 5.4 | 9.0 | 10.0 | 11.0 | 12.2 | 25.0 | 50.0 | 100.0 | 90 | 0.17 |
| 1/4-1 | 6.2 | 7.0 | 10.6 | 11.6 | 12.8 | 14.0 | 22.5 | 45.0 | 90.0 | 100 | 0.22 |
| 5/16-1 | 7.7 | 8.5 | 12.5 | 13.5 | 14.6 | 15.8 | 21.5 | 43.0 | 85.0 | 115 | 0.28 |
| 3/8-1 | 9.3 | 10.3 | 14.5 | 15.7 | 16.8 | 18.0 | 18.0 | 36.0 | 72.0 | 130 | 0.34 |
| 1/2-1 | 12.3 | 13.5 | 17.5 | 19.0 | 20.1 | 21.3 | 16.0 | 32.0 | 64.0 | 180 | 0.42 |
| 5/8-1 | 15.5 | 16.7 | 20.6 | 22.2 | 23.2 | 24.8 | 13.0 | 26.0 | 52.0 | 200 | 0.51 |
| 3/4-1 | 18.6 | 19.8 | 24.3 | 25.5 | 27.0 | 29.0 | 10.5 | 21.0 | 42.0 | 240 | 0.68 |
| 1-1 | 25.0 | 26.4 | 31.9 | 33.1 | 35.2 | 36.8 | 8.8 | 17.5 | 35.0 | 300 | 0.96 |
| 1 1/4-1 | 31.4 | 33.0 | 39.2 | 40.8 | 42.3 | 44.7 | 6.3 | 13.0 | 25.0 | 420 | 1.19 |
| 1 1/2-1 | 37.7 | 39.3 | 44.9 | 46.5 | 48.0 | 50.4 | 5.0 | 10.0 | 20.0 | 500 | 1.34 |
| 2-1 | 50.4 | 52.0 | 58.7 | 60.3 | 61.8 | 64.2 | 4.0 | 8.0 | 16.0 | 630 | 1.89 |
| 3/16-2 | 4.6 | 5.4 | 10.6 | 11.6 | 12.7 | 13.9 | 41.5 | 83.0 | 166.0 | 90 | 0.27 |
| 1/4-2 | 6.1 | 7.0 | 12.6 | 13.6 | 14.4 | 15.6 | 40.0 | 80.0 | 160.0 | 100 | 0.35 |
| 5/16-2 | 7.7 | 8.5 | 14.1 | 15.1 | 15.7 | 16.9 | 35.0 | 70.0 | 140.0 | 115 | 0.40 |
| 3/8-2 | 9.3 | 10.3 | 16.3 | 17.5 | 18.1 | 19.3 | 33.0 | 66.0 | 132.0 | 130 | 0.51 |
| 1/2-2 | 12.3 | 13.5 | 19.4 | 20.6 | 21.6 | 22.8 | 27.5 | 55.0 | 110.0 | 180 | 0.63 |
| 5/8-2 | 15.5 | 16.7 | 22.2 | 23.8 | 24.6 | 26.2 | 25.0 | 50.0 | 100.0 | 200 | 0.74 |
| 3/4-2 | 18.6 | 19.8 | 26.2 | 27.8 | 28.8 | 30.4 | 21.5 | 43.0 | 86.0 | 240 | 0.92 |
| 1-2 | 25.0 | 26.4 | 33.6 | 34.8 | 36.3 | 37.9 | 16.5 | 32.5 | 66.0 | 300 | 1.33 |
| 1 1/4-2 | 31.4 | 33.0 | 43.6 | 45.0 | 46.3 | 48.7 | 12.5 | 25.0 | 50.0 | 420 | 1.97 |
| 1 1/2-2 | 37.7 | 39.3 | 49.6 | 51.4 | 52.8 | 55.2 | 9.0 | 18.0 | 36.0 | 500 | 2.33 |
| 2-2 | 50.4 | 52.0 | 62.3 | 64.7 | 65.6 | 68.0 | 8.0 | 16.0 | 32.0 | 630 | 2.88 |

LT682

EN853 ST Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C to +100°C (-40°F to +212°F)

- Application:Suitable for conveying water-based,petroleum-based, and biodegradable hydraulic oil.

| Specification | I.D |  | W.D |  | O.D. |  | MaxW.P | P.P | Min.B.P. | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| 3/16-1 | 4.6 | 5.4 | 9.0 | 10.0 | 11.5 | 12.9 | 25.0 | 50.5 | 100.0 | 90 | 0.18 |
| 1/4-1 | 6.2 | 7.0 | 10.6 | 11.6 | 14.6 | 16.0 | 22.5 | 45.0 | 90.0 | 100 | 0.27 |
| 5/16-1 | 7.7 | 8.5 | 12.5 | 13.5 | 16.2 | 17.6 | 21.5 | 43.0 | 85.0 | 115 | 0.33 |
| 3/8-1 | 9.3 | 10.3 | 14.5 | 15.7 | 18.5 | 19.9 | 18.0 | 36.0 | 72.0 | 130 | 0.40 |
| 1/2-1 | 12.3 | 13.5 | 17.5 | 19.0 | 21.8 | 23.4 | 16.0 | 32.0 | 64.0 | 180 | 0.50 |
| 5/8-1 | 15.5 | 16.7 | 20.6 | 22.2 | 24.7 | 26.3 | 13.0 | 26.0 | 52.0 | 200 | 0.58 |
| 3/4-1 | 18.6 | 19.8 | 24.3 | 25.5 | 28.7 | 30.3 | 10.5 | 21.0 | 42.0 | 240 | 0.73 |
| 1-1 | 25.0 | 26.4 | 31.9 | 33.1 | 36.3 | 37.9 | 8.8 | 17.5 | 35.0 | 300 | 1.04 |
| 1 1/4-1 | 31.4 | 33.0 | 39.2 | 40.8 | 43.3 | 45.7 | 6.3 | 15.0 | 25.0 | 420 | 1.28 |
| 1 1/2-1 | 37.7 | 39.3 | 44.9 | 46.5 | 49.8 | 52.2 | 5.0 | 10.0 | 20.0 | 500 | 1.51 |
| 2-1 | 50.4 | 52.0 | 58.7 | 60.3 | 64.3 | 66.7 | 4.0 | 8.0 | 16.0 | 630 | 2.20 |
| 3/16-2 | 4.6 | 5.4 | 10.6 | 11.6 | 14.6 | 16.0 | 41.5 | 83.0 | 165.0 | 90 | 0.33 |
| 1/4-2 | 6.1 | 7.0 | 12.6 | 13.6 | 16.3 | 17.7 | 40.0 | 80.0 | 160.0 | 100 | 0.42 |
| 5/16-2 | 7.7 | 8.5 | 14.1 | 15.1 | 18 | 19.4 | 35.0 | 70.0 | 140.0 | 115 | 0.47 |
| 3/8-2 | 9.3 | 10.3 | 16.3 | 17.5 | 20.3 | 21.7 | 33.0 | 66.0 | 132.0 | 130 | 0.60 |
| 1/2-2 | 12.3 | 13.5 | 19.4 | 20.6 | 23.4 | 25.0 | 27.5 | 55.0 | 110.0 | 180 | 0.73 |
| 5/8-2 | 15.5 | 16.7 | 22.2 | 23.8 | 26.6 | 28.2 | 25.0 | 50.0 | 100.0 | 200 | 0.85 |
| 3/4-2 | 18.6 | 19.8 | 26.2 | 27.8 | 30.6 | 32.2 | 21.5 | 43.0 | 85.0 | 240 | 1.03 |
| 1-2 | 25.0 | 26.4 | 33.6 | 34.8 | 37.7 | 39.3 | 16.5 | 32.5 | 65.0 | 300 | 1.44 |
| 1 1/4-2 | 31.4 | 33.0 | 43.6 | 45.0 | 48.0 | 50.4 | 12.5 | 25.0 | 50.0 | 420 | 2.14 |
| 1 1/2-2 | 37.7 | 39.3 | 49.6 | 51.4 | 54.4 | 56.8 | 9.0 | 18.0 | 36.0 | 500 | 2.50 |
| 2-2 | 50.4 | 52.0 | 62.3 | 64.7 | 67.0 | 69.4 | 8.0 | 16.0 | 32.0 | 630 | 3.07 |

LT699

ISO 18752-AC/BC Artery Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:NBR synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire,one braid≥300,000 impulse cycles,two braids≥500,000 impulse cycles

- Outer Layer:skiving-free oil,abrasion,and weather resistant synthetic rubber

- Temperature Range:-40℃~+100℃(-40°F~+212°F);-55℃~+100℃(-67°F~+212°F)

- Application:Remarkable performance on high pressure and high impulse.Widely apply to excavator and other heavy duty construction machinery.

| SIZE | Specification | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.Impulse | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | 10K |  |  |
|  | SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |  |
|  | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | CYCLES | mm | kg/m |
| -4 | 1/4-1 | 5.8 | 6.5 | 10.7 | 11.7 | 12.9 | 13.9 | 25 | 50 | 100 | 30 | 80 | 0.20 |
| -5 | 5/16-1 | 7.7 | 8.5 | 12.5 | 13.5 | 14.7 | 15.7 | 25 | 50 | 100 | 30 | 92 | 0.25 |
| -6 | 3/8-1 | 9.8 | 10.5 | 14.5 | 15.5 | 16.9 | 17.9 | 21 | 42 | 84 | 30 | 104 | 0.32 |
| -8 | 1/2-1 | 12.8 | 13.5 | 17.7 | 18.7 | 20.2 | 21.2 | 18 | 36 | 72 | 30 | 144 | 0.40 |
| -10 | 5/8-1 | 15.8 | 16.6 | 20.7 | 21.7 | 23.5 | 24.5 | 14 | 28 | 56 | 30 | 160 | 0.50 |
| -12 | 3/4-1 | 18.8 | 19.8 | 24.4 | 25.4 | 27.0 | 29.0 | 14 | 28 | 56 | 30 | 192 | 0.67 |
| -16 | 1-1 | 24.8 | 25.8 | 32 | 33 | 35.4 | 36.6 | 9 | 18 | 36 | 30 | 240 | 0.91 |
| -20 | 11/4-1 | 31.4 | 33 | 39.3 | 40.7 | 42.7 | 44.3 | 6.3 | 13 | 25 | 30 | 400 | 1.19 |
| -24 | 11/2-1 | 37.7 | 39.3 | 45 | 46.4 | 48.4 | 50 | 5 | 10 | 20 | 30 | 480 | 1.33 |
| -32 | 2-1 | 50.4 | 52 | 58.8 | 60.2 | 62.2 | 63.8 | 4 | 8 | 16 | 30 | 560 | 1.87 |
| -4 | 1/4-2 | 5.8 | 6.5 | 12.6 | 13.6 | 14.5 | 15.5 | 42 | 84 | 168 | 50 | 80 | 0.35 |
| -5 | 5/16-2 | 7.7 | 8.5 | 14 | 15 | 15.8 | 16.8 | 35 | 84 | 140 | 50 | 92 | 0.40 |
| -6 | 3/8-2 | 9.8 | 10.5 | 16.4 | 17.4 | 18.2 | 19.2 | 35 | 70 | 140 | 50 | 104 | 0.52 |
| -8 | 1/2-2 | 12.8 | 13.5 | 19.5 | 20.5 | 21.7 | 22.7 | 28 | 56 | 112 | 50 | 144 | 0.63 |
| -10 | 5/8-2 | 15.8 | 16.6 | 22.5 | 23.5 | 24.9 | 25.9 | 28 | 56 | 112 | 50 | 160 | 0.76 |
| -12 | 3/4-2 | 18.8 | 19.8 | 26.5 | 27.5 | 29 | 30.2 | 25 | 50 | 100 | 50 | 192 | 0.94 |
| -16 | 1-2 | 24.8 | 25.8 | 33.5 | 34.5 | 36.5 | 37.7 | 21 | 42 | 84 | 50 | 240 | 1.37 |
| -20 | 11/4-2 | 31.4 | 33.0 | 43.5 | 44.9 | 46.7 | 48.3 | 14 | 28 | 56 | 50 | 400 | 2.00 |
| -24 | 11/2-2 | 37.7 | 39.3 | 49.8 | 51.2 | 53.2 | 54.8 | 9.0 | 18 | 36 | 50 | 480 | 2.30 |
| -32 | 2-2 | 50.4 | 52.0 | 62.5 | 63.9 | 66 | 67.6 | 8.0 | 16 | 32 | 50 | 610 | 3.02 |

LT683

EN857 SC Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:Black oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:black oil, weather, and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil

| Specification | I.D |  | W.D |  | O.D. |  | Max.W.P |  | P.P |  | Min.B.P. |  | Min.B.R. |  | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |  |  |  |  |
| IN | mm | mm | mm | mm | mm | mm | MPa | psi | MPa | psi | MPa | psi | inch | mm | kg/m |
| 1/4-1 | 6.1 | 6.9 | 9.9 | 10.9 | 11.8 | 13.2 | 22.5 | 3260 | 45.0 | 6265 | 90.0 | 13050 | 2.95 | 75 | 0.18 |
| 5/16-1 | 7.7 | 8.5 | 11.2 | 12.2 | 13.1 | 14.5 | 21.5 | 3120 | 43.0 | 6235 | 86.0 | 12470 | 3.35 | 85 | 0.20 |
| 3/8-1 | 9.3 | 10.1 | 13.3 | 14.3 | 15.1 | 16.5 | 18.0 | 2610 | 36.0 | 5220 | 72.0 | 10440 | 3.54 | 90 | 0.27 |
| 1/2-1 | 12.3 | 13.5 | 16.4 | 17.6 | 18.9 | 20.3 | 16.0 | 2320 | 32.0 | 4640 | 64.0 | 9280 | 5.12 | 130 | 0.35 |
| 5/8-1 | 15.5 | 16.7 | 19.8 | 21.0 | 21.9 | 23.3 | 13.0 | 1885 | 26.0 | 3770 | 52.0 | 7540 | 5.91 | 150 | 0.42 |
| 3/4-1 | 18.6 | 19.8 | 23.1 | 24.5 | 25.6 | 27.2 | 10.5 | 1520 | 21.0 | 3045 | 42.0 | 6090 | 7.09 | 180 | 0.54 |
| 1-1 | 25.0 | 26.4 | 30.5 | 31.9 | 33.2 | 34.8 | 8.8 | 1280 | 17.6 | 2550 | 35.5 | 5100 | 9.06 | 230 | 0.78 |
| 1/4-2 | 6.1 | 6.9 | 11.2 | 12.2 | 12.9 | 14.3 | 40.0 | 5800 | 80 | 11600 | 160.0 | 23200 | 2.96 | 75 | 0.28 |
| 5/16-2 | 7.7 | 8.5 | 12.8 | 13.8 | 14.5 | 15.9 | 35.0 | 5075 | 70 | 10150 | 140.0 | 20300 | 3.35 | 85 | 0.32 |
| 3/8-2 | 9.3 | 10.1 | 14.9 | 15.9 | 16.8 | 18.2 | 33 | 4785 | 66 | 9570 | 132.0 | 19140 | 3.54 | 90 | 0.43 |
| 1/2-2 | 12.3 | 13.5 | 18.0 | 19.2 | 20.0 | 21.6 | 27.5 | 3990 | 55 | 7975 | 110.0 | 15950 | 5.12 | 130 | 0.52 |
| 5/8-2 | 15.5 | 16.7 | 21.4 | 22.6 | 23.2 | 24.8 | 25 | 3625 | 50 | 7150 | 100.0 | 14500 | 6.69 | 170 | 0.66 |
| 3/4-2 | 18.6 | 19.8 | 25.0 | 26.4 | 27.4 | 29.0 | 21.5 | 3120 | 43 | 6235 | 86.0 | 12470 | 7.87 | 200 | 0.83 |
| 1-2 | 25.0 | 26.4 | 32.4 | 33.8 | 34.5 | 36.1 | 16.5 | 2390 | 33 | 4785 | 66.0 | 9570 | 9.84 | 250 | 1.17 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT685

MT/T98 Wire Braid Hydraulic Hose For Mining

- Hose Construction

- Inner Layer:black oil resistant synthetic rubber

- Reinforcement:one, two, or three braids of high tensile super flexible steel wire

- Outer Layer:black oil, weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying medium like mineral oil,water-based hydraulic oil,orwater in coalmining machinery such as coal mining hydraulic  supportand coal shearer

| SIZE | I.D mm |  | W.D mm |  | O.D mm |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| IN | Min | Max | Min | Max | Min | Max | MPa | MPa | MPa | mm | kg/m |
| 1/4-1 | 6.1 | 6.9 | 11.1 | 12.1 | 14.2 | 15.4 | 32 | 40 | 80 | 100 | 0.26 |
| 5/16-1 | 7.8 | 8.5 | 13.0 | 14.0 | 16.2 | 17.4 | 28 | 35 | 70 | 115 | 0.31 |
| 3/8-1 | 9.8 | 10.5 | 15.1 | 16.1 | 18.1 | 19.3 | 25.6 | 32 | 64 | 130 | 0.37 |
| 1:/2-1 | 12.8 | 13.5 | 18.9 | 19.9 | 21.9 | 23.1 | 22.4 | 33.6 | 56 | 180 | 0.48 |
| 5/8-1 | 15.8 | 16.6 | 22.0 | 23.0 | 24.7 | 26.3 | 16.8 | 21 | 42 | 205 | 0.57 |
| 3//4-1 | 18.8 | 19.8 | 25.0 | 26.0 | 27.6 | 29.2 | 14.4 | 18 | 36 | 240 | 0.66 |
| 7/8-1 | 21.8 | 22.8 | 28.0 | 29.0 | 30.6 | 32.2 | 12.8 | 16 | 32 | 280 | 0.73 |
| 1-1 | 25.0 | 26.0 | 31.3 | 32.5 | 34.2 | 35.8 | 11.2 | 14 | 28 | 300 | 0.86 |
| 11/4-1 | 31.6 | 33.6 | 38.3 | 39.9 | 41.8 | 44.2 | 9.0 | 11.5 | 22.5 | 420 | 1.15 |
| 11/2-1 | 37.7 | 39.8 | 44.8 | 46.4 | 48.1 | 50.3 | 7.0 | 9 | 17.5 | 500 | 1.29 |
| 13/4-1 | 44.6 | 45.6 | 51.8 | 53.4 | 55.4 | 57.6 | 5.0 | 8 | 12.5 | 550 | 1.55 |
| 2-1 | 50.7 | 52.0 | 57.8 | 59.4 | 61.3 | 63.7 | 3.0 | 6 | 7.5 | 630 | 1.77 |
| 1/4-2 | 6.1 | 6.9 | 12.9 | 13.9 | 16.0 | 17.2 | 60.0 | 75 | 150 | 100 | 0.40 |
| 5/16-2 | 7.8 | 8.5 | 14.9 | 15.9 | 18.0 | 19.2 | 48.0 | 60 | 120 | 115 | 0.47 |
| 3/8-2 | 9.8 | 10.5 | 16.6 | 17.6 | 19.9 | 21.1 | 40.0 | 50 | 100 | 130 | 0.55 |
| 1/2-2 | 12.8 | 13.5 | 20.7 | 21.7 | 23.7 | 24.9 | 36.0 | 45 | 90 | 180 | 0.71 |
| 5/8-2 | 15.8 | 16.6 | 23.4 | 24.6 | 26.5 | 28.1 | 32.0 | 40 | 80 | 205 | 0.86 |
| 3/4-2 | 18.8 | 19.8 | 26.4 | 27.6 | 29.4 | 31 | 25.0 | 31.5 | 62.5 | 240 | 0.95 |
| 7/8-2 | 21.8 | 22.8 | 29.5 | 30.7 | 32.3 | 34.1 | 22.0 | 27.5 | 55 | 280 | 1.05 |
| 1-2 | 25.0 | 26.0 | 32.8 | 34.0 | 36 | 37.6 | 21.0 | 26.5 | 52.5 | 300 | 1.25 |
| 11/4-2 | 31.6 | 33.6 | 39.8 | 41.4 | 43.6 | 45.8 | 17.0 | 21.5 | 42.5 | 420 | 1.57 |
| 11/2-2 | 37.7 | 39.8 | 46.4 | 48.0 | 49.8 | 52.2 | 12.0 | 15 | 30 | 500 | 1.88 |
| 13/4-2 | 44.6 | 45.6 | 53.4 | 55.0 | 56.8 | 59.2 | 9.0 | 13.5 | 22.5 | 55 | 2.13 |
| 2-2 | 50.7 | 52.0 | 59.4 | 61.0 | 62.8 | 65.2 | 8.0 | 12 | 20 | 630 | 2.45 |
| 5/16-3 | 7.8 | 8.5 | 16.5 | 17.5 | 19.6 | 20.8 | 50.0 | 75 | 125 | 115 | 0.61 |
| 3/8-3 | 9.8 | 10.5 | 18.0 | 19.2 | 21.5 | 22.7 | 45.0 | 62.5 | 112.5 | 130 | 0.69 |
| 1/2-3 | 12.8 | 13.5 | 22.1 | 23.3 | 25.5 | 26.7 | 40.0 | 56 | 100 | 180 | 0.94 |
| 5/8-3 | 15.8 | 16.6 | 25.1 | 26.3 | 28.3 | 29.9 | 35.0 | 43.5 | 87.5 | 205 | 1.16 |
| 3/4-3 | 18.8 | 19.8 | 28.1 | 29.3 | 31.2 | 32.8 | 28.0 | 35 | 70.5 | 240 | 1.26 |
| 7/8-3 | 21.8 | 22.8 | 31.1 | 32.3 | 34.2 | 35.8 | 25.0 | 31.5 | 62.5 | 280 | 1.43 |
| 1-3 | 25.0 | 26.0 | 34.6 | 35.6 | 37.2 | 38.8 | 24.0 | 30 | 60.5 | 300 | 1.59 |
| 11/4-3 | 31.6 | 33.6 | 41.4 | 43.0 | 45.4 | 47.6 | 19.0 | 24 | 47.5 | 420 | 2.05 |
| 11/2-3 | 37.7 | 39.8 | 48.0 | 49 | 51.8 | 54.2 | 15.0 | 19 | 37.5 | 500 | 2.44 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT686

MT/T98 Wire Braid Hydraulic Hose For Mining

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying medium like mineral oil,water-based hydraulic oil,or water in coal mining machinery such as coal mining hydraulic support and coal shearer.

| Specification | Specification | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| 64 | 2 1/2-1 | 63.5 | 65.3 | 71 | 73 | 76 | 80 | 3.5 | 5.25 | 10.5 | 800 | 2.42 |
| 76 | 3-1 | 75.5 | 77.5 | 83 | 85 | 88 | 92 | 3 | 4.5 | 9 | 920 | 2.86 |
| 85 | 3 3/8-1 | 84.5 | 86.7 | 92 | 94 | 97 | 101 | 2.5 | 3.75 | 7.5 | 1000 | 3.10 |
| 89 | 3 1/2-1 | 88.4 | 90 | 96.5 | 98.5 | 102 | 106 | 2.5 | 3.75 | 7.5 | 1100 | 3.34 |
| 102 | 4-1 | 101 | 104.5 | 110 | 115 | 116 | 121 | 2 | 3 | 6 | 1300 | 3.78 |
| 64 | 2 1/2-2 | 63.5 | 65.3 | 73 | 75 | 78 | 80 | 7 | 10.5 | 21 | 800 | 3.30 |
| 76 | 3-2 | 75.5 | 77.5 | 85 | 87 | 90 | 94 | 6 | 9 | 18 | 920 | 3.90 |
| 85 | 3 3/8-2 | 84.5 | 86.7 | 94 | 96 | 99 | 103 | 5 | 7.5 | 15 | 1000 | 4.30 |
| 89 | 3 1/2-2 | 88.4 | 90 | 98.5 | 100.5 | 104 | 108 | 5 | 7.5 | 15 | 1100 | 4.54 |
| 102 | 4-2 | 101 | 104.5 | 112 | 116 | 118 | 123 | 4 | 6 | 12 | 1300 | 5.50 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT687

SAE 100R16 Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:black hot oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40℃~+100℃(-40°F~+212°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.

| Specification | Specification | I.D |  | W.D |  | O.D |  | Max.W.P |  | P.P |  | Min.B.P |  | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | psi | MPa | psi | MPa | psi | mm | kg/m |
| -4 | 1/4 | 6.2 | 7.0 | 10.7 | 11.7 | 12.6 | 13.8 | 40 | 5800 | 80 | 11600 | 160 | 23200 | 50 | 0.3 |
| -5 | 5/16 | 7.7 | 8.5 | 12.1 | 13.3 | 14.4 | 15.6 | 35 | 5075 | 70 | 10150 | 140 | 20300 | 55 | 0.34 |
| -6 | 3/8 | 9.3 | 10.1 | 14.5 | 15.5 | 16.4 | 17.6 | 33 | 4785 | 66 | 9570 | 132 | 19140 | 65 | 0.42 |
| -8 | 1/2 | 12.3 | 13.5 | 17.9 | 18.9 | 19.9 | 21.1 | 27.5 | 3990 | 55 | 7975 | 110 | 15950 | 90 | 0.54 |
| -10 | 5/8 | 15.5 | 16.7 | 21.4 | 22.6 | 23.2 | 24.8 | 25 | 3625 | 50 | 7150 | 100 | 14500 | 100 | 0.68 |
| -12 | 3/4 | 18.6 | 19.8 | 25.1 | 26.3 | 27.2 | 28.8 | 21.5 | 3120 | 43 | 6235 | 86 | 12470 | 120 | 0.80 |
| -16 | 1 | 25.0 | 26.4 | 32.3 | 33.9 | 34.1 | 36.5 | 16.5 | 2390 | 33 | 4785 | 66 | 9570 | 150 | 1.15 |
| -20 | 1 1/4 | 31.4 | 33.0 | 40.3 | 41.9 | 42.8 | 45.2 | 12.5 | 1813 | 25 | 3625 | 50 | 7150 | 210 | 1.83 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT688

SAE 100R17 Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.

| Specification | Specification | I.D |  | W.D |  | O.D. |  | Max.W.P | P.P | Min.B.P. | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -4 | 1/4 | 6.2 | 7.0 | 10.3 | 11.3 | 12.2 | 13.4 | 21 | 42 | 84 | 50 | 0.19 |
| -5 | 5/16 | 7.7 | 8.5 | 11.8 | 12.8 | 13.7 | 14.9 | 21 | 42 | 84 | 55 | 0.22 |
| -6 | 3/8 | 9.3 | 10.1 | 13.6 | 14.6 | 15.5 | 16.7 | 21 | 42 | 84 | 65 | 0.28 |
| -8 | 1/2 | 12.3 | 13.5 | 16.8 | 17.8 | 19.4 | 20.6 | 21 | 42 | 84 | 90 | 0.38 |
| -10 | 5/8 | 15.5 | 16.7 | 22.2 | 23.2 | 23.9 | 25.1 | 21 | 42 | 84 | 100 | 0.68 |
| -12 | 3/4 | 18.6 | 19.8 | 25.1 | 26.3 | 26.9 | 28.5 | 21 | 42 | 84 | 120 | 0.83 |
| -16 | 1 | 25.5 | 26.4 | 33.2 | 34.4 | 35.7 | 37.3 | 21 | 42 | 84 | 150 | 1.29 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT689

SAE 100R19 Compact Wire Braid Hydraulic Hose

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying water-based,petroleum-based,and biodegradable hydraulic oil.

| Specification | Specification | I.D |  | W.D |  | O.D |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SIZE | SIZE | Min | Max | Min | Max | Min | Max |  |  |  |  |  |
| DASH | IN | mm | mm | mm | mm | mm | mm | MPa | MPa | MPa | mm | kg/m |
| -3 | 3/16 | 4.6 | 5.4 | 10.3 | 11.9 | 11.5 | 12.7 | 28 | 56 | 112 | 45 | 0.237 |
| -4 | 1/4 | 6.2 | 7.0 | 11.1 | 12.1 | 13.0 | 14.4 | 28 | 56 | 112 | 50 | 0.267 |
| -5 | 5/16 | 7.7 | 8.5 | 12.7 | 13.7 | 14.6 | 16.0 | 28 | 56 | 112 | 55 | 0.321 |
| -6 | 3/8 | 9.3 | 10.1 | 14.6 | 15.6 | 16.4 | 18.0 | 28 | 56 | 112 | 65 | 0.359 |
| -8 | 1/2 | 12.3 | 13.5 | 18.0 | 19.0 | 19.3 | 21.3 | 28 | 56 | 112 | 90 | 0.492 |
| -10 | 5/8 | 15.5 | 16.7 | 20.9 | 21.9 | 22.5 | 24.5 | 28 | 56 | 112 | 100 | 0.633 |
| -12 | 3/4 | 18.6 | 19.8 | 24.9 | 25.9 | 26.3 | 28.7 | 28 | 56 | 112 | 120 | 0.764 |
| -16 | 1 | 25.0 | 26.4 | 31.4 | 33.0 | 33.2 | 35.5 | 28 | 56 | 112 | 150 | 1011 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LTSA699

Exceeds ISO18752-BC Super Artery Wire Braid Hydraulic Hose

- Hose Construction

- Inner Layer:CR/NBR synthetic rubber

- Reinforcement:one or two braids of high tensile super flexible steel wire,
one braid≥300,000 impulse cycles,two braids≥500,000 impulse cycles

- Outer Layer:skiving-free oil,abrasion,and weather resistant synthetic rubber

- Temperature Range:-40°C ~ +120°C (-40°F ~ +248°F); -55°C ~ +100°C (-67°F ~ +212°F)

- Application:Remarkable performance on tight bend radius,high pressure,long service life,and high impulse,weather resistant for more than five years and warrantied for two years with Letone hose fittings and HNBR seals.Widely apply to excavator and other heavy duty construction machinery orhash working environment.

| TYPE | SIZE(inch) | I.D.(mm) | W.P.(MPa) | B.P.(MPa) | MIN.B.R.(mm) |
| --- | --- | --- | --- | --- | --- |
| SA699-1BC/CS | 1/4" | 6.4 | 29.5 | 118 | 40 |
| SA699-1BC/CS | 5/16" | 7.9 | 25 | 100 | 55 |
| SA699-1BC/CS | 3/8" | 9.5 | 23 | 92 | 65 |
| SA699-1BC/CS | 1/2" | 12.7 | 20 | 80 | 80 |
| SA699-1BC/CS | 5/8" | 15.9 | 15 | 60 | 105 |
| SA699-1BC/CS | 3/4" | 19 | 14 | 56 | 120 |
| SA699-1BC/CS | 1" | 25.4 | 11 | 44 | 160 |
| SA699-1BC/CS | 11/4" | 31.8 | 10 | 40 | 300 |
| SA699-1BC/CS | 11/2" | 38.1 | 5 | 20 | 480 |
| SA699-1BC/CS | 2" | 50.8 | 4 | 16 | 560 |
| SA699-2BC/CS | 1/4" | 6.4 | 42 | 168 | 55 |
| SA699-2BC/CS | 5/16" | 7.9 | 38 | 152 | 60 |
| SA699-2BC/CS | 3/8" | 9.5 | 35 | 140 | 70 |
| SA699-2BC/CS | 1/2" | 12.7 | 31 | 124 | 110 |
| SA699-2BC/CS | 5/8" | 15.9 | 28 | 112 | 130 |
| SA699-2BC/CS | 3/4" | 19 | 25 | 100 | 160 |
| SA699-2BC/CS | 1" | 25.4 | 21 | 84 | 210 |
| SA699-2BC/CS | 11/4" | 31.8 | 16.5 | 66 | 250 |
| SA699-2BC/CS | 11/2" | 38.1 | 13.5 | 54 | 300 |
| SA699-2BC/CS | 2" | 50.8 | 8 | 32 | 610 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.