LT800C

Grid-Connected Pipeline

- Hose Construction

- Inner Tube:EPDM rubber cured with peroxide

- Reinforcement:Multi-layer high-strength fiber braiding reinforced with spiralsteel wire

- Outer Layer:Corrugated black synthetic rubber(UL94VO flame-retardant)

- Temperature Range:-40℃~+93℃(-40°F~+200°F)

- Color:black

- Application:Suitable for conveyingfluid media such as air,water,water-glycol, oil-water emulsion, antifreeze fluid,phosphate esterhydraulicoil,etc.

| Size | I.D |  | O.D |  | W.P |  | B.R | Vac. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | in | mm | in | mm | PSI | Mpa | mm | in Hg | KG/M |
| -12 | 3/4" | 19.1 | 1.15 | 29.1 | 150 | 1.03 | 19.1 | 29 | 0.501 |
| -16 | 1" | 25.4 | 1.39 | 35.4 | 150 | 1.03 | 25.4 | 29 | 0.630 |
| -20 | 11/4" | 31.8 | 1.65 | 419 | 150 | 1.03 | 31.8 | 29 | 0.793 |
| -24 | 11/2" | 38.1 | 1.90 | 48.2 | 150 | 103 | 38.1 | 29 | 0.923 |
| -32 | 2" | 50.8 | 2.44 | 61.9 | 150 | 1.03 | 50.8 | 29 | 1.266 |
| -40 | 21/2" | 63.5 | 3.00 | 76.3 | 150 | 1.03 | 63.5 | 29 | 1.859 |
| -48 | 3" | 76.2 | 3.50 | 89.0 | 150 | 1.03 | 76.2 | 29 | 2.213 |
| -64 | 4" | 1,016 | 4.53 | 115.1 | 150 | 1.03 | 1,016 | 29 | 3.142 |

The items marked with * are for reference only; the actual specifications are subject to the pipe body.

LT800B

Grid-Connected Pipeline

- Hose Construction

- Inner Tube:EPDM rubber cured with peroxide

- Reinforcement:One-layer high-strength fiber braiding reinforced

- OuterLayer:black synthetic rubber(UL94VO flame-retardant)

- Temperature Range:-40℃~+99℃(-40°F~+210°F)

- Color:black

- Application:Suitable for conveying fluid media such as air,water,water-glycol,oil-water emulsion, antifreeze fluid,phosphate esterhydraulic oil,etc.

| Size | I.D |  | O.D |  | W.P |  | B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | in | mm | in | mm | PSI | Mpa | mm | KG/M |
| -16 | 1" | 25.4 | 1.47 | 37.3 | 200 | 1.38 | 127.0 | 0.73 |
| -24 | 11/2" | 38.1 | 2.08 | 52.8 | 200 | 1.38 | 203.2 | 1.31 |
| -32 | 2" | 50.8 | 2.52 | 64.0 | 200 | 1.38 | 304.8 | 1.40 |

The items marked with * are for reference only; the actual specifications are subject to the pipe body.

LT800A

LCP-Water Manifold Jumper Hose

- Hose Construction

- Inner Tube:EPDM rubber cured with peroxide

- Reinforcement:One layers of braided synthetic fiber

- Outer Cover:Black weather-resistant, ozone-resistant, UL94V0 flame-retardant special synthetic rubber

- Temperature Range:-40°C~+120°C (-40°F~+248°F)

- Color:red、black、blue

- Application:Suitable for medium fluids such as air, water, water glycol, oil-water emulsion, antifreeze, phosphate ester hydraulic oil, etc.

| Size |  | I.D | 0.D | Max.W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | mm | mm | MPa | MPa | mm | kg/m |
| -4 | 1/4 | 6.4 | 12.1 | 1 | 4 | 25.4 | 0.13 |
| -5 | 5/16 | 7.7 | 14.5 | 1 | 4 | 31.5 | 0.18 |
| -6 | 3/8 | 9.5 | 15.9 | 1 | 4 | 38.1 | 0.19 |
| -8 | 1/2 | 12.7 | 19.8 | 1 | 4 | 69.9 | 0.25 |
| -10 | 5/8 | 15.9 | 23.1 | 7 | 4 | 88.9 | 0.30 |
| -12 | 3/4 | 19.1 | 26.2 | 1 | 4 | 114.3 | 0.35 |
| -16 | 1 | 25.4 | 32.6 | 0.7 | 2.8 | 152.4 | 0.52 |
| -20 | 1 1/4 | 31.8 | 43 | 0.7 | 2.8 | 195 | 0.70 |

The items marked with * are for reference only; the actual specifications are subject to the pipe body.

LT781

SAE 100R3 Fiber Braid Hose

- Hose Construction

- Inner Tube:blackoil resistant synthetic rubber

- Reinforcement:two braids of textile

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to convey medium like petroleum based hydraulic oil,lubrication oil,water,and air.

| SIZE (Dash) | SIZE (in.) | I.D. (mm) |  | O.D. (mm) |  | Max.W.P. | Min.B.P. | Min.B.R. | W.T |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | (MPa) | (MPa) | (mm) | kg/m | 1bft |
| -3 | 3/16 | 4.6 | 5.5 | 11.9 | 13.6 | 10.5 | 42 | 75 | 0.15 | 0.14 |
| -4 | 1/4 | 6.1 | 7.0 | 13.4 | 15.1 | 8.7 | 34.8 | 75 | 0.16 | 0.16 |
| -5 | 5/16 | 7.4 | 8.5 | 16.7 | 18.3 | 8.4 | 33.6 | 100 | 0 .25 | 0.21 |
| -6 | 3/8 | 9.3 | 10.1 | 18.3 | 19.8 | 7.8 | 31.2 | 100 | 0.31 | 0.26 |
| -8 | 1/2 | 12.3 | 13.5 | 22.8 | 24.6 | 7 | 28 | 125 | 0.40 | 0.38 |
| -10 | 5/8 | 15.5 | 16.7 | 26.2 | 27.8 | 6.1 | 24.4 | 140 | 0.51 | 0.42 |
| -12 | 3/4 | 18.5 | 19.8 | 30.7 | 32.5 | 5.2 | 20.8 | 150 | 0.61 | 0.58 |
| -16 | 1 | 25.1 | 26.2 | 36.8 | 39.2 | 3.9 | 15.6 | 205 | 0.91 | 0.74 |
| -20 | 1 1/4 | 31.4 | 32.9 | 42.8 | 45.2 | 2.6 | 10.4 | 250 | 1.10 | 0.77 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT782

SAE 100R4 Hydraulic Suction And Return Line

- Hose Construction

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one or two braids of textile and a helical spiral-wire

- Outer Layer:black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to convey medium like petroleum based hydraulic oil,lubrication oil,water,and air.

| SIZE |  | I.D mm |  | O.D mm | Max.W.P |  | P.P |  | Min.B.P |  | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Max | MPa | psi | MPa | psi | MPa | psi | kg/m |
| -12 | 3/4 | 18.2 | 19.8 | 34.0 | 2.1 | 305 | 4.2 | 610 | 8.4 | 1210 | 0.68 |
| -16 | 1 | 24.6 | 26.2 | 40.0 | 1.7 | 250 | 3.5 | 510 | 7 | 1015 | 0.84 |
| -20 | 11/4 | 30.6 | 33.0 | 48.0 | 1.4 | 200 | 2.8 | 410 | 5.6 | 810 | 1.13 |
| -24 | 11/2 | 36.9 | 39.3 | 54.0 | 1.05 | 150 | 2.1 | 305 | 4.2 | 610 | 1.41 |
| -32 | 2 | 49.2 | 52.4 | 68.0 | 0.7 | 100 | 1.4 | 200 | 2.8 | 410 | 1.85 |
| -40 | 21/2 | 61.9 | 65.1 | 81.0 | 0.4 | 60 | 0.85 | 120 | 1.7 | 250 | 2.28 |
| -48 | 3 | 74.6 | 77.8 | 93.0 | 0.4 | 60 | 0.8 | 120 | 1.6 | 230 | 2.64 |
| -56 | 31/2 | 87.3 | 90.5 | 106.0 | 0.3 | 40 | 0.6 | 90 | 1.25 | 180 | 3.02 |
| -64 | 4 | 100.0 | 103.2 | 120.0 | 0.25 | 40 | 0.6 | 70 | 1 | 145 | 3.21 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT783

SAE 100R5 Hydraulic Hose

- Inner Tube:black oil resistant synthetic rubber

- Reinforcement:one braid of high tensile steel wire

- Outer Layer:textile braid impregnated with synthetic rubber

- Temperature Range:-40℃to+135℃(-40°F to 275°F),except air(not to exceed +93℃)and water(not to exceed+100℃)

- Application:Suitable for conveying medium like petroleum based hydraulicoil,lubrication oil,water,and air.

| SIZE (Dash) | SIZE (mm) | I.D. (mm) |  | O.D. (mm) |  | Max.W.P. | Min.B.P. | P.P | Min.B.R.* | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | (MPa) | (MPa) | (MPa) | (mm) | kg/m |
| -4 | 5 | 4.8 | 5.5 | 12.5 | 13.7 | 21 | 84 | 42 | 75 | 0.20 |
| -5 | 6.3 | 6.4 | 7.2 | 14.1 | 15.3 | 21 | 84 | 42 | 85 | 0.26 |
| -6 | 8 | 7.9 | 8.7 | 16.2 | 17.6 | 15.7 | 62.8 | 31.4 | 100 | 0.32 |
| -8 | 11 | 10.3 | 11.1 | 18.4 | 20.0 | 14 | 56 | 28 | 115 | 0.37 |
| -10 | 12.5 | 12.7 | 13.7 | 22.2 | 24.0 | 12.2 | 48.8 | 24.4 | 140 | 0.51 |
| -12 | 16 | 15.9 | 17.0 | 26.2 | 28.0 | 10.5 | 42 | 21 | 165 | 0.65 |
| -16 | 22 | 22.2 | 23.3 | 30.0 | 32.2 | 5.6 | 22.4 | 11.2 | 185 | 0.69 |
| -20 | 29 | 28.6 | 29.8 | 36.3 | 38.9 | 4.3 | 17.2 | 8.6 | 230 | 0.85 |
| -24 | 35 | 34.9 | 36.1 | 42.8 | 45.2 | 3.5 | 14.0 | 7 | 265 | 1.04 |
| -32 | 46 | 46.0 | 47.2 | 54.3 | 57.6 | 2.4 | 9.6 | 4.8 | 335 | 1.46 |
| -40 | 60 | 60.3 | 61.9 | 70.8 | 74.2 | 2.4 | 9.6 | 4.8 | 610 | 2.10 |
| -48 | 76 | 76.2 | 77.8 | 88.3 | 91.7 | 1.4 | 5.6 | 2.8 | 840 | 2.86 |

The items marked with * are for reference only; the actual specifications are subject to the hose body.

LT784

SAE 100R6 Fiber Braid Hose

- Hose Construction

- Inner Tube:Black oil-resistant synthetic rubber

- Reinforcement:One braid of textile

- Outer Layer:Black oil, weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable for conveying medium like petroleum based hydraulic oil, lubrication oil,water,and air

| SIZE |  | I.D. mm |  | O.D. mm |  | Max.W.P. |  | Min.B.P. |  | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Min | Max | MPa | psi | MPa | psi | mm | kg/m |
| -3 | 3/16 | 4.6 | 5.5 | 11.0 | 12.2 | 3.4 | 500 | 13.6 | 2000 | 50 | 0.10 |
| -4 | 1/4 | 6.1 | 6.9 | 12.4 | 13.6 | 2.8 | 400 | 11.2 | 1600 | 65 | 0.13 |
| -5 | 5/16 | 7.4 | 8.5 | 14.2 | 15.4 | 2.8 | 400 | 11.2 | 1600 | 80 | 0.16 |
| -6 | 3/8 | 9.3 | 10.1 | 15.7 | 16.9 | 2.8 | 400 | 11.2 | 1600 | 80 | 0.18 |
| -8 | 1/2 | 12.3 | 13.5 | 19.5 | 21.1 | 2.8 | 400 | 11.2 | 1600 | 100 | 0.25 |
| -10 | 5/8 | 15.5 | 16.7 | 22.7 | 24.3 | 2.4 | 340 | 9.6 | 1360 | 125 | 0.29 |
| -12 | 3/4 | 18.2 | 19.8 | 26.2 | 27.8 | 2.1 | 340 | 8.4 | 1200 | 150 | 0.37 |

Note: The actual parameters are subject to the final atlas

LT785

GB1186 Compressed Air Hose

- Hose Construction

- Inner Tube:Black synthetic rubber

- Reinforcement:One or two braids of textile

- Outer Layer:Weather and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +70°C (-40°F ~ +158°F)

- Application:Suitable to all kinds of power machinery and pneumatic tools to convey compressed air water or noble gases under the normal temperature

| SIZE |  | I.D mm |  | O.D mm | Max.W.P | Min.B.P | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Min | MPa | MPa | Kg/m |
| -8 | 1/2 | 12.5 | 14.0 | 23 | 1.0 | 4.0 | 0.34 |
| -10 | 5/8 | 15.5 | 17.0 | 26 | 1.0 | 4.0 | 0.40 |
| -12 | 3/4 | 18.5 | 20.0 | 29 | 1.0 | 4.0 | 0.45 |
| -16 | 1 | 24.5 | 26.0 | 35 | 1.0 | 4.0 | 0.48 |
| -20 | 11/4 | 31.5 | 33.0 | 45 | 1.0 | 4.0 | 0.95 |
| -24 | 11/2 | 37.5 | 39.0 | 52 | 1.0 | 4.0 | 1.25 |
| -32 | 2 | 50.0 | 52.5 | 66 | 1.0 | 4.0 | 1.60 |
| -8 | 1/2 | 12.5 | 14.0 | 23 | 2.0 | 8.0 | 0.34 |
| -10 | 5/8 | 15.5 | 17.0 | 26 | 2.0 | 8.0 | 0.41 |
| -12 | 3/4 | 18.5 | 20.0 | 29 | 2.0 | 8.0 | 0.46 |
| -16 | 1 | 24.5 | 26.0 | 35 | 2.0 | 8.0 | 0.50 |
| -20 | 11/4 | 31.5 | 33.0 | 45 | 2.0 | 8.0 | 0.97 |
| -24 | 11/2 | 37.5 | 39.0 | 52 | 2.0 | 8.0 | 1.27 |
| -32 | 2 | 50.0 | 52.5 | 66 | 2.0 | 8.0 | 1.70 |

Note: The actual parameters are subject to the final atlas

LT787

EN854 2TE&3TE Oil Return Line

- Hose Construction

- Inner Tube:Black oil resistant synthetic rubber

- Reinforcement:One or two braids of textile

- Outer Layer:Black oil,weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to convey petroleum-based hydraulic oil,crude oil,fuel oil, lubricating oil,emulsified oil, air,and water

| SIZE |  | I.D. mm |  | O.D. mm |  | Max.W.P. | P.P | Min.B.P. | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Min | Max | MPa | MPa | MPa | mm | kg/m |
| -4 | 1/4-1 | 6.1 | 6.9 | 12.4 | 13.6 | 7.5 | 15 | 30 | 40 | 0.14 |
| -5 | 5/16-1 | 7.4 | 8.5 | 14.2 | 15.4 | 6.8 | 13.6 | 27.2 | 50 | 0.16 |
| -6 | 3/8-1 | 9.3 | 10.1 | 16.0 | 17.2 | 6.3 | 12.6 | 25.2 | 60 | 0.18 |
| -8 | 1/2-1 | 12.3 | 13.5 | 18.9 | 20.5 | 5.8 | 11.6 | 23.2 | 70 | 0.22 |
| -10 | 5/8-1 | 15.5 | 16.7 | 23.0 | 24.6 | 5.0 | 10 | 20.0 | 90 | 0.30 |
| -12 | 3/4-1 | 18.5 | 19.8 | 26.4 | 28.0 | 4.5 | 9 | 18.0 | 110 | 0.33 |
| -16 | 1-1 | 24.6 | 26.2 | 33.3 | 35.7 | 4.0 | 8 | 16.0 | 130 | 0.46 |
| -20 | 1 1/4-1 | 30.8 | 32.8 | 40.8 | 43.2 | 3.5 | 7 | 14.0 | 140 | 0.22 |
| -24 | 1/4-2 | 6.1 | 6.9 | 13.9 | 15.1 | 14.5 | 29 | 58 | 45 | 0.19 |
| -32 | 5/16-2 | 7.4 | 8.5 | 16.2 | 17.4 | 13.0 | 26 | 52 | 55 | 0.23 |
| -6 | 3/8-2 | 9.3 | 10.1 | 17.9 | 19.1 | 11.0 | 22 | 44.4 | 70 | 0.26 |
| -8 | 1/2-2 | 12.3 | 13.5 | 21.0 | 22.6 | 9.3 | 18.6 | 37.2 | 85 | 0.30 |
| -10 | 5/8-2 | 15.5 | 16.7 | 25.4 | 27.0 | 8.0 | 16 | 32.0 | 105 | 0.41 |
| -12 | 3/4-2 | 18.2 | 19.8 | 28.2 | 29.8 | 7.0 | 14 | 28.0 | 130 | 0.47 |
| -16 | 1-2 | 24.6 | 26.2 | 35.3 | 37.7 | 5.5 | 11 | 22.0 | 150 | 0.69 |
| -20 | 1 1/4-2 | 30.8 | 32.8 | 40.8 | 43.2 | 4.5 | 9 | 18.0 | 190 | 0.73 |
| -24 | 1 1/2-2 | 37.1 | 39.1 | 47.8 | 50.2 | 4.0 | 8 | 16.0 | 240 | 0.87 |
| -32 | 2-2 | 50.0 | 52.0 | 60.8 | 64.0 | 3.0 | 6 | 13.2 | 300 | 1.16 |

Note: The actual parameters are subject to the final atlas

LT788

Sand Blastlng Hose

- Hose Construction

- Inner Tube:Black abrasion resistant synthetic rubber (UPE layer is available)

- Reinforcement:Braided fiber or steel wire

- Outer Layer:Black weather and abrasion resistant synthetic rubber

- Temperature Range:-40℃~+70℃(-40°F~+158°F)

- Application:Apply to industries like railway,shipbuilding,and construction to remove rust on the metal surface

| SIZE |  | I.D mm |  | O.D mm |  | Max.W.P | P.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Min | Max | Min | MPa | MPa | mm | kg/m |
| -10 | 5/8 | 15.5 | 16.7 | 28.2 | 29.8 | 1.0 | 2.0 | 4.0 | 105 | 0.98 |
| -12 | 3/4 | 18.8 | 19.8 | 34.2 | 35.8 | 1.0 | 2.0 | 4.0 | 130 | 1.14 |
| -16 | 1 | 24.8 | 25.8 | 42.8 | 45.2 | 1.0 | 2.0 | 4.0 | 150 | 1.50 |
| -20 | 1 1/4 | 31.6 | 32.6 | 48.8 | 51.5 | 1.0 | 2.0 | 4.0 | 190 | 1.80 |
| -24 | 1 1/2 | 37.7 | 38.8 | 57.5 | 60.5 | 1.0 | 2.0 | 4.0 | 240 | 2.10 |
| -28 | 1 3/4 | 44.6 | 45.6 | 62.5 | 65.5 | 1.0 | 2.0 | 4.0 | 260 | 2.30 |
| -32 | 2 | 50.7 | 52 | 69.5 | 72.5 | 1.0 | 2.0 | 4.0 | 300 | 2.75 |
| -40 | 2 1/2 | 63.7 | 65.3 | 83.5 | 86.5 | 0.8 | 1.6 | 3.2 | 800 | 3.50 |
| -48 | 3 | 75.5 | 77.3 | 100.0 | 104.0 | 0.8 | 1.6 | 3.2 | 920 | 4.50 |
| -56 | 3 1/2 | 88.5 | 90.5 | 113.0 | 117.0 | 0.8 | 1.6 | 3.2 | 1100 | 5.50 |
| -64 | 4 | 101.5 | 104 | 126.0 | 130.0 | 0.8 | 1.6 | 3.2 | 1300 | 6.50 |

Note: The actual parameters are subject to the final atlas

LT780

Oil Return Rubber Hose

- Hose Construction

- Inner Tube:Black oil resistant synthetic rubber

- Reinforcement:One braid or one spiral of textile

- Outer Layer:Black oil weather,and abrasion resistant synthetic rubber

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to convey petroleum-based hydraulic oil, lubricating oil,water,and air

| SIZE |  | I.D mm |  | O.D mm |  | Max.W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | Min | Max | Min | Max | MPa | MPa | mm | Kg/m |
| -4 | 1/4" | 6.3 | 6.9 | 12.4 | 13.6 | 2 | 8 | 65 | 0.138 |
| -5 | 5/16" | 7.8 | 8.5 | 14.8 | 16.0 | 2 | 8 | 80 | 0.18 |
| -6 | 3/8" | 9.5 | 10.8 | 16.4 | 17.6 | 2 | 8 | 80 | 0.189 |
| -8 | 1/2" | 12.5 | 13.8 | 21.7 | 23.3 | 2 | 8 | 100 | 0.339 |
| -10 | 5/8" | 15.8 | 16.6 | 25.7 | 27.3 | 2 | 8 | 125 | 0.443 |
| -12 | 3/4" | 18.8 | 19.8 | 28.9 | 30.5 | 2 | 8 | 150 | 0.528 |
| -14 | 7/8" | 21.8 | 22.8 | 31.2 | 32.8 | 2 | 8 | 170 | 0.535 |
| -16 | 1" | 25.2 | 26.2 | 34.4 | 36.0 | 2 | 8 | 200 | 0.59 |
| -20 | 1-1/4" | 31.8 | 32.8 | 43.8 | 46.2 | 2 | 8 | 250 | 0.954 |
| -24 | 1-1/2" | 37.8 | 38.8 | 50.8 | 53.2 | 2 | 8 | 300 | 1.189 |
| -32 | 2" | 50.8 | 52.2 | 64.3 | 66.7 | 2 | 8 | 360 | 1.612 |
| -40 | 2-1/2" | 63.8 | 65.5 | 78.8 | 81.2 | 2 | 6 | 430 | 2.272 |
| -48 | 3" | 75.8 | 77.5 | 90.8 | 93.2 | 2 | 6 | 500 | 2.693 |

Note: The actual parameters are subject to the final atlas