LT799

Ultra-High Pressure Thermoplastic Hose

- Hose Construction

- Inner Layer:nylon

- Reinforcement:4~8 plies of spiraled steel wire

- Outer Layer:super abrasion resistant polyurethane

- Temperature Range:-30°C~+80°C(-22°F~+176°F)

- Application:Suitable to transfer water,oil and other medium under high pressure,widely apply to the industries like high pressure spraying,high pressure cleaning,sandblasting,engineering machinery, agricultural machinery,forestry machinery,petrochemical,etc.

| SIZE |  | I.D | 0.D | Max.W.P |  | Min.B.P |  | Min.B.R |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | mm | mm | bar | psi | bar | psi | mm |
| -2 | 1/8-2 | 3.5 | 7.2 | 1040 | 15000 | 2600 | 37700 | 60 |
| - | 5/32-2 | 4.1 | 9.8 | 1200 | 17400 | 3000 | 43500 | 65 |
| -3 | 3/16-2 | 5.2 | 10.8 | 1040 | 15000 | 2600 | 37700 | 70 |
| -4 | 1/4-2 | 6.4 | 11.5 | 1040 | 15000 | 2600 | 37700 | 85 |
| -5 | 5/16-2 | 7.9 | 13.4 | 1040 | 15000 | 2600 | 37700 | 100 |
| -6 | 3/8-2 | 9.9 | 16.4 | 690 | 10000 | 1725 | 25000 | 140 |
| -8 | 1/2-2 | 12.8 | 20.4 | 690 | 10000 | 1725 | 25000 | 200 |
|  | 5/32-4 | 4 | 12.0 | 2200 | 31900 | 5500 | 79750 | 90 |
| -3 | 3/16-4 | 5.1 | 12.8 | 1800 | 26100 | 4500 | 65250 | 95 |
| -4 | 1/4-4 | 6.3 | 14.3 | 1640 | 23700 | 4100 | 59450 | 100 |
| -5 | 5/16-4 | 8.2 | 16.6 | 1500 | 21700 | 3750 | 54375 | 105 |
| -6 | 3/8-4 | 9.9 | 18.8 | 1400 | 20300 | 3500 | 50750 | 110 |
| -8 | 1/2-4 | 12.8 | 22.5 | 1400 | 20300 | 3500 | 50750 | 120 |
| - | 5/32-6 | 4 | 11.8 | 2800 | 40600 | 7000 | 101500 | 140 |
| -3 | 3/16-6 | 5 | 14.8 | 2500 | 36200 | 6250 | 90625 | 200 |
| -4 | 1/4-6 | 6.3 | 16.0 | 2500 | 36200 | 6250 | 90625 | 210 |
| -5 | 5/16-6 | 7.9 | 19.0 | 2500 | 36200 | 6250 | 90625 | 220 |
| -6 | 3/8-6 | 9.9 | 20.8 | 2070 | 30000 | 5175 | 75000 | 250 |
| -8 | 1/2-6 | 12.8 | 27.0 | 1800 | 26100 | 4500 | 65250 | 290 |
| -12 | 3/4-6 | 18.8 | 35.0 | 1600 | 23200 | 4000 | 58000 | 350 |
| -3 | 3/16-8 | 4.7 | 16.0 | 4000 | 58000 | 10000 | 145000 | 200 |
| -4 | 1/4-8 | 6.3 | 18.0 | 3500 | 50750 | 8750 | 126875 | 230 |
| -5 | 5/16-8 | 7.6 | 21.5 | 3200 | 55100 | 8000 | 116000 | 280 |
| -8 | 1/2-8 | 12.8 | 28.7 | 3000 | 43600 | 7500 | 108750 | 350 |

LT790

SAE 100R7 Fiber Braid High Pressure Thermoplastic Hose

- Hose Construction

- Inner Tube:Nylon

- Reinforcement:One or two braids of synthetic fiber

- Outer Layer:Polyurethane

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to transfer petroleum and water hydraulic oil,which could be used as lubrication lines and blowout preventer lines,etc,widely apply to hydraulic lifts,agricultural machines and construction machines

| SIZE |  | I.D. | O.D. | Max.W.P. |  | Min.B.P. |  | MIN.B.R. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dash | In. | mm | mm | MPa | Psi | MPa | Psi | mm |
| -3 | 3/16-1 | 4.8 | 10.3 | 21 | 3045 | 84 | 12180 | 35 |
| -4 | 1/4-1 | 6.3 | 12.7 | 22.5 | 3260 | 90 | 13050 | 50 |
| -5 | 5/16-1 | 7.9 | 14.3 | 19 | 2755 | 76 | 11020 | 50 |
| -6 | 3/8-1 | 9.5 | 15.9 | 17.5 | 2540 | 70 | 10160 | 80 |
| -8 | 1/2-1 | 12.7 | 19.8 | 14 | 2030 | 56 | 8120 | 100 |
| -3 | 3/16-2 | 4.8 | 10.3 | 25 | 3620 | 100 | 14480 | 55 |
| -4 | 1/4-2 | 6.3 | 13.3 | 27.4 | 3980 | 109.6 | 15920 | 75 |
| -5 | 5/16-2 | 7.9 | 15 | 26 | 3770 | 104 | 15080 | 85 |
| -6 | 3/8-2 | 9.5 | 18 | 25 | 3620 | 100 | 14480 | 100 |
| -8 | 1/2-2 | 12.7 | 21.6 | 21 | 3040 | 84 | 12160 | 140 |
| -10 | 5/8-2 | 15.9 | 23.6 | 16 | 2320 | 64 | 9280 | 165 |
| -12 | 3/4-2 | 19 | 26.4 | 14 | 2030 | 56 | 8120 | 195 |
| -16 | 1-2 | 25.4 | 34 | 10.5 | 1520 | 42 | 6080 | 256 |

Note: The actual parameters are subject to the final atlas

LT791

SAE 100R7 Wire Braid High Pressure Thermoplastic Hose

- Hose Construction

- Inner Tube:Nylon

- Reinforcement:One or two braids of steel wire

- Outer Layer:Polyurethane

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to transfer petroleum and water hydraulic oil,which could be used as lubrication lines and blowout preventer lines,etc,widely apply to hydraulic lifts,agricultural machines and construction machines

| SIZE |  | I.D. | O.D. | Max.W.P. |  | Min.B.P. |  | MIN.B.R. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dash | In. | mm | mm | MPa | psi | MPa | psi | mm |
| -3 | 3/16-1 | 4.8 | 9.8 | 35 | 5070 | 140 | 20280 | 30 |
| -4 | 1/4-1 | 6.3 | 12.7 | 27.5 | 3990 | 110 | 15960 | 40 |
| -5 | 5/16-1 | 7.9 | 14.3 | 25 | 3620 | 100 | 14480 | 55 |
| -6 | 3/8-1 | 9.5 | 15.9 | 22.5 | 3260 | 63.6 | 13040 | 65 |
| -8 | 1/2-1 | 12.7 | 19.8 | 17.5 | 2540 | 70 | 10160 | 85 |
| -10 | 5/8-1 | 15.9 | 23.3 | 14 | 2030 | 56 | 8120 | 115 |
| -12 | 3/4-1 | 19 | 26.5 | 12 | 1740 | 48 | 6960 | 140 |
| -16 | 1-1 | 25.4 | 34 | 10 | 1450 | 40 | 5800 | 180 |
| -4 | 1/4-2 | 6.3 | 13.3 | 35 | 5070 | 140 | 20280 | 40 |
| -5 | 5/16-2 | 7.9 | 14.9 | 32.5 | 4710 | 130 | 18840 | 50 |
| -6 | 3/8-2 | 9.5 | 16.7 | 29 | 4200 | 116 | 16800 | 70 |
| -8 | 1/2-2 | 12.7 | 19.8 | 26 | 3770 | 104 | 15080 | 80 |
| -10 | 5/8-2 | 15.9 | 23.3 | 20 | 2900 | 80 | 11600 | 130 |
| -12 | 3/4-2 | 19 | 26 | 17.5 | 2540 | 70 | 10160 | 160 |
| -16 | 1-2 | 25.4 | 33 | 12 | 1740 | 48 | 6960 | 220 |

Note: The actual parameters are subject to the final atlas

LT794

SAE 100R8 Aramid Fiber Braid High Pressure Thermoplastic Hose

- Hose Construction

- Inner Tube:Nylon

- Reinforcement:One or two braids of aramid fiber

- Outer Layer:Polyurethane

- Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)

- Application:Suitable to transfer petroleum and water hydraulic oil,which could be used as lubrication lines and blowout preventer lines,etc,widely apply to hydraulic lifts,agricultural machines and construction machines

| SIZE |  | I.D | O.D | Max.W.P |  | Min.B.P |  | Min.B.R |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DASH | IN | mm | mm | MPa | psi | MPa | psi | mm |
| -3 | 3/16-2 | 4.8 | 10.3 | 35 | 5070 | 140 | 20280 | 35 |
| -4 | 1/4-2 | 6.3 | 12.3 | 37.5 | 5440 | 150 | 21760 | 40 |
| -5 | 5/16-2 | 7.9 | 14.3 | 32.5 | 4710 | 130 | 18840 | 45 |
| -6 | 3/8-2 | 9.5 | 16.7 | 28 | 4060 | 112 | 16240 | 60 |
| -8 | 1/2-2 | 12.7 | 22.5 | 35 | 5070 | 140 | 20280 | 80 |
| -10 | 5/8-2 | 15.9 | 24.5 | 22.5 | 3260 | 90 | 13040 | 120 |
| -12 | 3/4-2 | 19 | 28 | 17.5 | 2540 | 70 | 10160 | 140 |
| -16 | 1-2 | 25.4 | 34 | 15 | 2170 | 60 | 8680 | 160 |

Note: The actual parameters are subject to the final atlas