LT799
Ultra-High Pressure Thermoplastic Hose
· Hose Construction
· [bookmark: _GoBack]Inner Layer:nylon
· Reinforcement:4~8 plies of spiraled steel wire
· Outer Layer:super abrasion resistant polyurethane
· Temperature Range:-30°C~+80°C(-22°F~+176°F)
· Application:Suitable to transfer water,oil and other medium under high pressure,widely apply to the industries like high pressure spraying,high pressure cleaning,sandblasting,engineering machinery, agricultural machinery,forestry machinery,petrochemical,etc.
	SIZE
	I.D
	0.D
	Max.W.P
	Min.B.P
	Min.B.R

	DASH
	IN
	mm
	mm
	bar
	psi
	bar
	psi
	mm

	-2
	1/8-2
	3.5
	7.2
	1040
	15000
	2600
	37700
	60

	-
	5/32-2
	4.1
	9.8
	1200
	17400
	3000
	43500
	65

	-3
	3/16-2
	5.2
	10.8
	1040
	15000
	2600
	37700
	70

	-4
	1/4-2
	6.4
	11.5
	1040
	15000
	2600
	37700
	85

	-5
	5/16-2
	7.9
	13.4
	1040
	15000
	2600
	37700
	100

	-6
	3/8-2
	9.9
	16.4
	690
	10000
	1725
	25000
	140

	-8
	1/2-2
	12.8
	20.4
	690
	10000
	1725
	25000
	200

	 
	5/32-4
	4
	12.0
	2200
	31900
	5500
	79750
	90

	-3
	3/16-4
	5.1
	12.8
	1800
	26100
	4500
	65250
	95

	-4
	1/4-4
	6.3
	14.3
	1640
	23700
	4100
	59450
	100

	-5
	5/16-4
	8.2
	16.6
	1500
	21700
	3750
	54375
	105

	-6
	3/8-4
	9.9
	18.8
	1400
	20300
	3500
	50750
	110

	-8
	1/2-4
	12.8
	22.5
	1400
	20300
	3500
	50750
	120

	-
	5/32-6
	4
	11.8
	2800
	40600
	7000
	101500
	140

	-3
	3/16-6
	5
	14.8
	2500
	36200
	6250
	90625
	200

	-4
	1/4-6
	6.3
	16.0
	2500
	36200
	6250
	90625
	210

	-5
	5/16-6
	7.9
	19.0
	2500
	36200
	6250
	90625
	220

	-6
	3/8-6
	9.9
	20.8
	2070
	30000
	5175
	75000
	250

	-8
	1/2-6
	12.8
	27.0
	1800
	26100
	4500
	65250
	290

	-12
	3/4-6
	18.8
	35.0
	1600
	23200
	4000
	58000
	350

	-3
	3/16-8
	4.7
	16.0
	4000
	58000
	10000
	145000
	200

	-4
	1/4-8
	6.3
	18.0
	3500
	50750
	8750
	126875
	230

	-5
	5/16-8
	7.6
	21.5
	3200
	55100
	8000
	116000
	280

	-8
	1/2-8
	12.8
	28.7
	3000
	43600
	7500
	108750
	350


LT790
SAE 100R7 Fiber Braid High Pressure Thermoplastic Hose
· Hose Construction
· Inner Tube:Nylon
· Reinforcement:One or two braids of synthetic fiber 
· Outer Layer:Polyurethane
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable to transfer petroleum and water hydraulic oil,which could be used as lubrication lines and blowout preventer lines,etc,widely apply to hydraulic lifts,agricultural machines and construction machines
	SIZE
	I.D.
	O.D.
	Max.W.P.
	Min.B.P.
	MIN.B.R.

	Dash
	In.
	mm
	mm
	MPa
	Psi
	MPa
	Psi
	mm

	-3
	3/16-1
	4.8
	10.3
	21
	3045
	84
	12180
	35

	-4
	1/4-1
	6.3
	12.7
	22.5
	3260
	90
	13050
	50

	-5
	5/16-1
	7.9
	14.3
	19
	2755
	76
	11020
	50

	-6
	3/8-1
	9.5
	15.9
	17.5
	2540
	70
	10160
	80

	-8
	1/2-1
	12.7
	19.8
	14
	2030
	56
	8120
	100

	-3
	3/16-2
	4.8
	10.3
	25
	3620
	100
	14480
	55

	-4
	1/4-2
	6.3
	13.3
	27.4
	3980
	109.6
	15920
	75

	-5
	5/16-2
	7.9
	15
	26
	3770
	104
	15080
	85

	-6
	3/8-2
	9.5
	18
	25
	3620
	100
	14480
	100

	-8
	1/2-2
	12.7
	21.6
	21
	3040
	84
	12160
	140

	-10
	5/8-2
	15.9
	23.6
	16
	2320
	64
	9280
	165

	-12
	3/4-2
	19
	26.4
	14
	2030
	56
	8120
	195

	-16
	1-2
	25.4
	34
	10.5
	1520
	42
	6080
	256


Note: The actual parameters are subject to the final atlas
LT791
SAE 100R7 Wire Braid High Pressure Thermoplastic Hose
· Hose Construction
· Inner Tube:Nylon
· Reinforcement:One or two braids of steel wire
· Outer Layer:Polyurethane
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable to transfer petroleum and water hydraulic oil,which could be used as lubrication lines and blowout preventer lines,etc,widely apply to hydraulic lifts,agricultural machines and construction machines
	SIZE
	I.D.
	O.D.
	Max.W.P.
	Min.B.P.
	MIN.B.R.

	Dash
	In.
	mm
	mm
	MPa
	psi
	MPa
	psi
	mm

	-3
	3/16-1
	4.8
	9.8
	35
	5070
	140
	20280
	30

	-4
	1/4-1
	6.3
	12.7
	27.5
	3990
	110
	15960
	40

	-5
	5/16-1
	7.9
	14.3
	25
	3620
	100
	14480
	55

	-6
	3/8-1
	9.5
	15.9
	22.5
	3260
	63.6
	13040
	65

	-8
	1/2-1
	12.7
	19.8
	17.5
	2540
	70
	10160
	85

	-10
	5/8-1
	15.9
	23.3
	14
	2030
	56
	8120
	115

	-12
	3/4-1
	19
	26.5
	12
	1740
	48
	6960
	140

	-16
	1-1
	25.4
	34
	10
	1450
	40
	5800
	180

	-4
	1/4-2
	6.3
	13.3
	35
	5070
	140
	20280
	40

	-5
	5/16-2
	7.9
	14.9
	32.5
	4710
	130
	18840
	50

	-6
	3/8-2
	9.5
	16.7
	29
	4200
	116
	16800
	70

	-8
	1/2-2
	12.7
	19.8
	26
	3770
	104
	15080
	80

	-10
	5/8-2
	15.9
	23.3
	20
	2900
	80
	11600
	130

	-12
	3/4-2
	19
	26
	17.5
	2540
	70
	10160
	160

	-16
	1-2
	25.4
	33
	12
	1740
	48
	6960
	220


Note: The actual parameters are subject to the final atlas
LT794
SAE 100R8 Aramid Fiber Braid High Pressure Thermoplastic Hose
· Hose Construction
· Inner Tube:Nylon
· Reinforcement:One or two braids of aramid fiber
· Outer Layer:Polyurethane
· Temperature Range:-40°C ~ +100°C (-40°F ~ +212°F)
· Application:Suitable to transfer petroleum and water hydraulic oil,which could be used as lubrication lines and blowout preventer lines,etc,widely apply to hydraulic lifts,agricultural machines and construction machines
	SIZE
	I.D
	O.D
	Max.W.P
	Min.B.P
	Min.B.R

	DASH
	IN
	mm
	mm
	MPa
	psi
	MPa
	psi
	mm

	-3
	3/16-2
	4.8
	10.3
	35
	5070
	140
	20280
	35

	-4
	1/4-2
	6.3
	12.3
	37.5
	5440
	150
	21760
	40

	-5
	5/16-2
	7.9
	14.3
	32.5
	4710
	130
	18840
	45

	-6
	3/8-2
	9.5
	16.7
	28
	4060
	112
	16240
	60

	-8
	1/2-2
	12.7
	22.5
	35
	5070
	140
	20280
	80

	-10
	5/8-2
	15.9
	24.5
	22.5
	3260
	90
	13040
	120

	-12
	3/4-2
	19
	28
	17.5
	2540
	70
	10160
	140

	-16
	1-2
	25.4
	34
	15
	2170
	60
	8680
	160


Note: The actual parameters are subject to the final atlas
