LT801

Wire Braid Air Hose

- Application:Designed for higher pressure air transfer services in construction and mining industries,suitable for extremely environment because of its abrasion resistant characteristic

- Hose Construction

- Inner Tube:Black NR&SBR synthetic rubber

- Reinforcement:One braid of high tensile super flexible steel wire

- Outer Layer:Black or yellow NR&SBR synthetic rubber

- Temperature Range:-30℃~82℃(-22°F~180°F)

- *The hose dimension,pressure and color can be customized based on the requirements

| I.D. |  | O.D. |  | W.P | Min.B.P | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 1/2 | 13 | 0.87 | 22 | 600 | 2400 | 180 | 0.42 |
| 3/4 | 19 | 1.10 | 28 | 600 | 2400 | 240 | 0.55 |
| 1 | 25 | 1.34 | 34 | 600 | 2400 | 300 | 0.70 |
| 1-1/4 | 32 | 1.65 | 42 | 600 | 2400 | 420 | 1.07 |
| 1-1/2 | 38 | 1.89 | 48 | 600 | 2400 | 500 | 1.28 |
| 2 | 51 | 2.52 | 64 | 600 | 2400 | 630 | 1.99 |
| 2.5 | 64 | 3.26 | 77 | 450 | 1800 | 800 | 2.44 |
| 3 | 76 | 3.54 | 90 | 450 | 1800 | 920 | 2.90 |
| 4 | 102 | 4.65 | 118 | 450 | 1800 | 1300 | 5.16 |

LT803

GB/T 1186 Fiber Spiral Compressed Air Hose

- Application:Designed for compressed air transfer in construction  and mining industries,suitable for extremely environment because of its abrasion resistant characteristic

- Hose Construction

- Inner Tube:Black NR&SBR synthetic rubber

- Reinforcement:Multi-spiral  high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Black NR&SBR or CR synthetic rubber

- Temperature Range:-30℃~82℃(-22°F~180°F)

- *The hose dimension,pressure and color can be customized based on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.52 | 64 | 150 | 375 | 400 | 1.55 |
| 2.5 | 64 | 3.03 | 77 | 150 | 375 | 500 | 2.25 |
| 3 | 76 | 3.58 | 91 | 150 | 375 | 570 | 2.60 |
| 4 | 102 | 4.80 | 122 | 150 | 375 | 750 | 4.5 |
| 2 | 51 | 2.64 | 67 | 230 | 575 | 400 | 1.65 |
| 2.5 | 64 | 3.15 | 80 | 230 | 575 | 500 | 2.35 |
| 3 | 76 | 3.70 | 94 | 230 | 575 | 570 | 2.70 |
| 4 | 102 | 4.92 | 125 | 230 | 575 | 750 | 4.60 |
| 2 | 51 | 2.75 | 70 | 360 | 900 | 400 | 1.75 |
| 2.5 | 64 | 3.26 | 83 | 360 | 900 | 500 | 2.45 |
| 3 | 76 | 3.82 | 97 | 360 | 900 | 570 | 2.80 |
| 4 | 102 | 5.03 | 128 | 360 | 900 | 750 | 4.70 |

LT805

GB/T 1186 Fiber Spiral High-Temp Compressed Air Hose

- Application:Designed for compressed air transfer in construction and mining industries,suitable for the relatively high-temperature environment.

- Hose Construction

- Inner Tube:Black high-temp resistant synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Black high-temp resistant synthetic rubber

- Temperature Range:-30℃~150℃(-22°F~302°F)

- *The hose  dimension,pressure and color can be customized based on there quirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.52 | 64 | 150 | 375 | 400 | 1.55 |
| 2.5 | 64 | 3.03 | 77 | 150 | 375 | 500 | 2.25 |
| 3 | 76 | 3.58 | 91 | 150 | 375 | 570 | 2.60 |
| 4 | 102 | 4.80 | 122 | 150 | 375 | 750 | 4.5 |
| 2 | 51 | 2.64 | 67 | 230 | 575 | 400 | 1.65 |
| 2.5 | 64 | 3.15 | 80 | 230 | 575 | 500 | 2.35 |
| 3 | 76 | 3.70 | 94 | 230 | 575 | 570 | 2.70 |
| 4 | 102 | 4.92 | 125 | 230 | 575 | 750 | 4.60 |
| 2 | 51 | 2.75 | 70 | 360 | 900 | 400 | 1.75 |
| 2.5 | 64 | 3.26 | 83 | 360 | 900 | 500 | 2.45 |
| 3 | 76 | 3.82 | 97 | 360 | 900 | 570 | 2.80 |
| 4 | 102 | 5.03 | 128 | 360 | 900 | 750 | 4.70 |