LT801
Wire Braid Air Hose
· Application:Designed for higher pressure air transfer services in construction and mining industries,suitable for extremely environment because of its abrasion resistant characteristic
· Hose Construction
· Inner Tube:Black NR&SBR synthetic rubber
· Reinforcement:One braid of high tensile super flexible steel wire
· Outer Layer:Black or yellow NR&SBR synthetic rubber
· Temperature Range:-30℃~82℃(-22°F~180°F)
· *The hose dimension,pressure and color can be customized based on the requirements
	[bookmark: _GoBack]I.D.
	O.D.
	W.P
	Min.B.P
	Min.B.R.
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	1/2
	13
	0.87
	22
	600
	2400
	180
	0.42

	3/4
	19
	1.10
	28
	600
	2400
	240
	0.55

	1
	25
	1.34
	34
	600
	2400
	300
	0.70

	1-1/4
	32
	1.65
	42
	600
	2400
	420
	1.07

	1-1/2
	38
	1.89
	48
	600
	2400
	500
	1.28

	2
	51
	2.52
	64
	600
	2400
	630
	1.99

	2.5
	64
	3.26
	77
	450
	1800
	800
	2.44

	3
	76
	3.54
	90
	450
	1800
	920
	2.90

	4
	102
	4.65
	118
	450
	1800
	1300
	5.16


LT803
GB/T 1186 Fiber Spiral Compressed Air Hose
· Application:Designed for compressed air transfer in construction  and mining industries,suitable for extremely environment because of its abrasion resistant characteristic
· Hose Construction
· Inner Tube:Black NR&SBR synthetic rubber
· Reinforcement:Multi-spiral  high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Black NR&SBR or CR synthetic rubber
· Temperature Range:-30℃~82℃(-22°F~180°F)
· *The hose dimension,pressure and color can be customized based on the requirements.
	I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.52
	64
	150
	375
	400
	1.55

	2.5
	64
	3.03
	77
	150
	375
	500
	2.25

	3
	76
	3.58
	91
	150
	375
	570
	2.60

	4
	102
	4.80
	122
	150
	375
	750
	4.5

	2
	51
	2.64
	67
	230
	575
	400
	1.65

	2.5
	64
	3.15
	80
	230
	575
	500
	2.35

	3
	76
	3.70
	94
	230
	575
	570
	2.70

	4
	102
	4.92
	125
	230
	575
	750
	4.60

	2
	51
	2.75
	70
	360
	900
	400
	1.75

	2.5
	64
	3.26
	83
	360
	900
	500
	2.45

	3
	76
	3.82
	97
	360
	900
	570
	2.80

	4
	102
	5.03
	128
	360
	900
	750
	4.70


LT805
GB/T 1186 Fiber Spiral High-Temp Compressed Air Hose
· Application:Designed for compressed air transfer in construction and mining industries,suitable for the relatively high-temperature environment.
· Hose Construction
· Inner Tube:Black high-temp resistant synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Black high-temp resistant synthetic rubber
· Temperature Range:-30℃~150℃(-22°F~302°F)
· *The hose  dimension,pressure and color can be customized based on there quirements.
	I.D
	O.D
	W.P
	Min.B.P
	Min.B.R.
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.52
	64
	150
	375
	400
	1.55

	2.5
	64
	3.03
	77
	150
	375
	500
	2.25

	3
	76
	3.58
	91
	150
	375
	570
	2.60

	4
	102
	4.80
	122
	150
	375
	750
	4.5

	2
	51
	2.64
	67
	230
	575
	400
	1.65

	2.5
	64
	3.15
	80
	230
	575
	500
	2.35

	3
	76
	3.70
	94
	230
	575
	570
	2.70

	4
	102
	4.92
	125
	230
	575
	750
	4.60

	2
	51
	2.75
	70
	360
	900
	400
	1.75

	2.5
	64
	3.26
	83
	360
	900
	500
	2.45

	3
	76
	3.82
	97
	360
	900
	570
	2.80

	4
	102
	5.03
	128
	360
	900
	750
	4.70



