LT901

HG/T 3035 General Purpose Water Suction&Discharge Rubber Hose

- Application:Designed for the general use of construction,agriculture,and other industrial applications.

- Hose Construction

- Inner Tube:Black EPDM or NR&SBR synthetic rubber(UPE layer is available)

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Black EPDM or NR&SBR synthetic rubber

- Temperature Range:-30°℃~100℃(-22°F~212°F)

- *The hose dimension,pressure and color can be customized based on the requirements.

| I.D. |  | O.D. |  | Max.W.P. | Min.B.P | Min.B.R. | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.64 | 67 | 150 | 375 | 350 | 1.65 |
| 2.5 | 64 | 3.15 | 80 | 150 | 375 | 450 | 2.35 |
| 3 | 76 | 3.66 | 93 | 150 | 375 | 520 | 2.70 |
| 4 | 102 | 4.80 | 122 | 150 | 375 | 700 | 4.60 |
| 5 | 127 | 5.87 | 149 | 150 | 375 | 950 | 6.45 |
| 6 | 152 | 6.81 | 173 | 150 | 375 | 1160 | 7.00 |
| 8 | 203 | 9.17 | 233 | 150 | 375 | 1400 | 15.00 |
| 10 | 254 | 11.30 | 287 | 150 | 375 | 1700 | 20.00 |
| 2 | 51 | 2.76 | 70 | 300 | 750 | 370 | 2.05 |
| 2.5 | 64 | 3.27 | 83 | 300 | 750 | 470 | 2.75 |
| 3 | 76 | 3.78 | 96 | 300 | 750 | 540 | 3.10 |
| 4 | 102 | 4.92 | 125 | 300 | 750 | 720 | 5.00 |
| 5 | 127 | 6.10 | 155 | 300 | 750 | 970 | 7.25 |
| 6 | 152 | 7.05 | 179 | 300 | 750 | 1180 | 7.90 |
| 8 | 203 | 9.41 | 239 | 300 | 750 | 1450 | 15.90 |
| 10 | 254 | 11.54 | 293 | 300 | 750 | 1750 | 20.90 |

LT903

HG/T 3035 Water Discharge Rubber Hose

- Application:Designed for the general use of construction,agriculture,and other industrial applications.

- Hose Construction

- Inner Tube:Black EPDM or NR&SBR synthetic rubber (UPE layer is available)

- Reinforcement:Multi-spiral high tensile synthetic fibers

- Outer Layer:Oil,abrasion resistant,anti-aging black,gray or blue NBR or PVC synthetic rubber

- Temperature Range:-30°C〜82°C (-22°F~180°F)

- *The hose dimension,pressure and color can be customized  based on  the  requirements.

| I.D |  | O.D |  | W.P | Min.B.P | W.T |
| --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | kg/m |
| 2 | 51 | 2.40 | 61 | 45 | 113 | 1.40 |
| 2.5 | 64 | 2.91 | 74 | 45 | 113 | 2.10 |
| 3 | 76 | 3.43 | 87 | 45 | 113 | 2.45 |
| 4 | 102 | 4.57 | 116 | 45 | 113 | 4.35 |
| 5 | 127 | 5.51 | 140 | 45 | 113 | 6.20 |
| 6 | 152 | 6.46 | 164 | 45 | 113 | 6.75 |
| 8 | 203 | 8.82 | 224 | 45 | 113 | 14.75 |
| 10 | 254 | 10.94 | 278 | 45 | 113 | 19.75 |
| 2 | 51 | 2.40 | 61 | 75 | 188 | 1.40 |
| 2.5 | 64 | 2.91 | 74 | 75 | 188 | 2.10 |
| 3 | 76 | 3.43 | 87 | 75 | 188 | 2.45 |
| 4 | 102 | 4.57 | 116 | 75 | 188 | 4.35 |
| 5 | 127 | 5.51 | 140 | 75 | 188 | 6.20 |
| 6 | 152 | 6.46 | 164 | 75 | 188 | 6.75 |
| 8 | 203 | 8.82 | 224 | 75 | 188 | 14.75 |
| 10 | 254 | 10.94 | 278 | 75 | 188 | 19.75 |
| 2 | 51 | 2.48 | 63 | 150 | 375 | 1.50 |
| 2.5 | 64 | 2.99 | 76 | 150 | 375 | 2.20 |
| 3 | 76 | 3.50 | 89 | 150 | 375 | 2.55 |
| 4 | 102 | 4.65 | 118 | 150 | 375 | 4.45 |
| 5 | 127 | 5.59 | 142 | 150 | 375 | 6.30 |
| 6 | 152 | 6.54 | 166 | 150 | 375 | 6.85 |
| 8 | 203 | 8.90 | 226 | 150 | 375 | 14.85 |
| 10 | 254 | 11.02 | 280 | 150 | 375 | 19.85 |