LT901
HG/T 3035 General Purpose Water Suction&Discharge Rubber Hose
· Application:Designed for the general use of construction,agriculture,and other industrial applications.
· [bookmark: _GoBack]Hose Construction
· Inner Tube:Black EPDM or NR&SBR synthetic rubber(UPE layer is available)
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Black EPDM or NR&SBR synthetic rubber
· Temperature Range:-30°℃~100℃(-22°F~212°F)
· *The hose dimension,pressure and color can be customized based on the requirements.
	I.D.
	O.D.
	Max.W.P.
	Min.B.P
	Min.B.R.
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.64
	67
	150
	375
	350
	1.65

	2.5
	64
	3.15
	80
	150
	375
	450
	2.35

	3
	76
	3.66
	93
	150
	375
	520
	2.70

	4
	102
	4.80
	122
	150
	375
	700
	4.60

	5
	127
	5.87
	149
	150
	375
	950
	6.45

	6
	152
	6.81
	173
	150
	375
	1160
	7.00

	8
	203
	9.17
	233
	150
	375
	1400
	15.00

	10
	254
	11.30
	287
	150
	375
	1700
	20.00

	2
	51
	2.76
	70
	300
	750
	370
	2.05

	2.5
	64
	3.27
	83
	300
	750
	470
	2.75

	3
	76
	3.78
	96
	300
	750
	540
	3.10

	4
	102
	4.92
	125
	300
	750
	720
	5.00

	5
	127
	6.10
	155
	300
	750
	970
	7.25

	6
	152
	7.05
	179
	300
	750
	1180
	7.90

	8
	203
	9.41
	239
	300
	750
	1450
	15.90

	10
	254
	11.54
	293
	300
	750
	1750
	20.90


LT903
HG/T 3035 Water Discharge Rubber Hose
· Application:Designed for the general use of construction,agriculture,and other industrial applications.
· Hose Construction
· Inner Tube:Black EPDM or NR&SBR synthetic rubber (UPE layer is available)
· Reinforcement:Multi-spiral high tensile synthetic fibers
· Outer Layer:Oil,abrasion resistant,anti-aging black,gray or blue NBR or PVC synthetic rubber
· Temperature Range:-30°C〜82°C (-22°F~180°F)
· *The hose dimension,pressure and color can be customized  based on  the  requirements.
	I.D
	O.D
	W.P
	Min.B.P
	W.T

	in
	mm
	in
	mm
	psi
	psi
	kg/m

	2
	51
	2.40
	61
	45
	113
	1.40

	2.5
	64
	2.91
	74
	45
	113
	2.10

	3
	76
	3.43
	87
	45
	113
	2.45

	4
	102
	4.57
	116
	45
	113
	4.35

	5
	127
	5.51
	140
	45
	113
	6.20

	6
	152
	6.46
	164
	45
	113
	6.75

	8
	203
	8.82
	224
	45
	113
	14.75

	10
	254
	10.94
	278
	45
	113
	19.75

	2
	51
	2.40
	61
	75
	188
	1.40

	2.5
	64
	2.91
	74
	75
	188
	2.10

	3
	76
	3.43
	87
	75
	188
	2.45

	4
	102
	4.57
	116
	75
	188
	4.35

	5
	127
	5.51
	140
	75
	188
	6.20

	6
	152
	6.46
	164
	75
	188
	6.75

	8
	203
	8.82
	224
	75
	188
	14.75

	10
	254
	10.94
	278
	75
	188
	19.75

	2
	51
	2.48
	63
	150
	375
	1.50

	2.5
	64
	2.99
	76
	150
	375
	2.20

	3
	76
	3.50
	89
	150
	375
	2.55

	4
	102
	4.65
	118
	150
	375
	4.45

	5
	127
	5.59
	142
	150
	375
	6.30

	6
	152
	6.54
	166
	150
	375
	6.85

	8
	203
	8.90
	226
	150
	375
	14.85

	10
	254
	11.02
	280
	150
	375
	19.85



