LT1102
Oil & Dairy Food & Beverage Hose
· Application:Suitable for animal oil,edible oil and dairy products transfer.
· Hose Construction
· Inner Tube:White oil resistant NBR synthetic rubber, compliance with FDA and 3A requirements
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Gray or blue synthetic rubber
· Temperature Range:-30℃~100℃(-22°F~212°F)
· *The hose dimension,pressure and color can be customized based on the requirements.
	[bookmark: _GoBack]I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	1/2
	13
	0.9
	22.5
	300
	1200
	130
	0.35

	5/8
	16
	1
	26
	300
	1200
	150
	0.45

	3/4
	19
	1.3
	32
	300
	1200
	180
	0.6

	1
	25
	1.5
	38
	300
	1200
	200
	0.94

	1-1/4
	32
	1.8
	45
	300
	1200
	250
	1.2

	1-1/2
	38
	2
	52
	300
	1200
	300
	1.5

	2
	51
	2.52
	64
	150
	375
	400
	1.55

	3
	76
	3.70
	94
	150
	375
	570
	2.65

	4
	102
	4.72
	120
	150
	375
	750
	4.55

	2
	51
	2.64
	67
	300
	750
	400
	1.65

	3
	76
	3.82
	97
	300
	750
	570
	2.75

	4
	102
	4.84
	123
	300
	750
	750
	4.65


LT1103
Dry Goods Food & Beverage Hose
· Application:Suitable for the  bulk transfer of flour and  edible grains.
· Hose Construction
· Inner Tube:White abrasion resistant NR&SBR synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Abrasion resistant,anti-aging gray or blue NR&SBR synthetic rubber
· Temperature Range:-30°℃~82℃(-22°F~180°F)
· *The hose dimension,pressure  and  color can  be customized  based  on  the  requirements
	I.D
	O.D
	Max.W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	1/2
	13
	0.9
	22.5
	300
	1200
	130
	0.35

	5/8
	16
	1
	26
	300
	1200
	150
	0.45

	3/4
	19
	1.3
	32
	300
	1200
	180
	0.6

	1
	25
	1.5
	38
	300
	1200
	200
	0.94

	1-1/4
	32
	1.8
	45
	300
	1200
	250
	1.2

	1-1/2
	38
	2
	52
	300
	1200
	300
	1.5

	2
	51
	2.64
	67
	150
	375
	400
	1.65

	3
	76
	3.82
	97
	150
	375
	570
	2.75

	4
	102
	4.84
	123
	150
	375
	750
	4.65

	2
	51
	2.76
	70
	300
	750
	400
	1.75

	3
	76
	3.94
	100
	300
	750
	570
	2.85

	4
	102
	4.96
	126
	300
	750
	750
	4.75


LT1104
Beverage Transfer Hose
· Application:Suitable for the transfer of milk,juice,alcohol,and other beverages.
· Hose Construction
· Inner Tube:White EPDM synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Gray or blue EPDM synthetic rubber
· Temperature Range:-30°℃~100℃(-22°F~212°F)
· *The hose dimension,pressure and color can be customized based on the requirements
	I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	1/2
	13
	0.9
	22.5
	300
	1200
	130
	0.35

	5/8
	16
	1
	26
	300
	1200
	150
	0.45

	3/4
	19
	1.3
	32
	300
	1200
	180
	0.6

	1
	25
	1.5
	38
	300
	1200
	200
	0.94

	1-1/4
	32
	1.8
	45
	300
	1200
	250
	1.2

	1-1/2
	38
	2
	52
	300
	1200
	300
	1.5

	2
	51
	2.52
	64
	150
	375
	400
	1.55

	3
	76
	3.70
	94
	150
	375
	570
	2.65

	4
	102
	4.72
	120
	150
	375
	750
	4.55

	2
	51
	2.64
	67
	300
	750
	400
	1.65

	3
	76
	3.82
	97
	300
	750
	570
	2.75

	4
	102
	4.84
	123
	300
	750
	750
	4.65



