LT1102

Oil & Dairy Food & Beverage Hose

- Application:Suitable for animal oil,edible oil and dairy products transfer.

- Hose Construction

- Inner Tube:White oil resistant NBR synthetic rubber, compliance with FDA and 3A requirements

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Gray or blue synthetic rubber

- Temperature Range:-30℃~100℃(-22°F~212°F)

- *The hose dimension,pressure and color can be customized based on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 1/2 | 13 | 0.9 | 22.5 | 300 | 1200 | 130 | 0.35 |
| 5/8 | 16 | 1 | 26 | 300 | 1200 | 150 | 0.45 |
| 3/4 | 19 | 1.3 | 32 | 300 | 1200 | 180 | 0.6 |
| 1 | 25 | 1.5 | 38 | 300 | 1200 | 200 | 0.94 |
| 1-1/4 | 32 | 1.8 | 45 | 300 | 1200 | 250 | 1.2 |
| 1-1/2 | 38 | 2 | 52 | 300 | 1200 | 300 | 1.5 |
| 2 | 51 | 2.52 | 64 | 150 | 375 | 400 | 1.55 |
| 3 | 76 | 3.70 | 94 | 150 | 375 | 570 | 2.65 |
| 4 | 102 | 4.72 | 120 | 150 | 375 | 750 | 4.55 |
| 2 | 51 | 2.64 | 67 | 300 | 750 | 400 | 1.65 |
| 3 | 76 | 3.82 | 97 | 300 | 750 | 570 | 2.75 |
| 4 | 102 | 4.84 | 123 | 300 | 750 | 750 | 4.65 |

LT1103

Dry Goods Food & Beverage Hose

- Application:Suitable for the  bulk transfer of flour and  edible grains.

- Hose Construction

- Inner Tube:White abrasion resistant NR&SBR synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Abrasion resistant,anti-aging gray or blue NR&SBR synthetic rubber

- Temperature Range:-30°℃~82℃(-22°F~180°F)

- *The hose dimension,pressure  and  color can  be customized  based  on  the  requirements

| I.D |  | O.D |  | Max.W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 1/2 | 13 | 0.9 | 22.5 | 300 | 1200 | 130 | 0.35 |
| 5/8 | 16 | 1 | 26 | 300 | 1200 | 150 | 0.45 |
| 3/4 | 19 | 1.3 | 32 | 300 | 1200 | 180 | 0.6 |
| 1 | 25 | 1.5 | 38 | 300 | 1200 | 200 | 0.94 |
| 1-1/4 | 32 | 1.8 | 45 | 300 | 1200 | 250 | 1.2 |
| 1-1/2 | 38 | 2 | 52 | 300 | 1200 | 300 | 1.5 |
| 2 | 51 | 2.64 | 67 | 150 | 375 | 400 | 1.65 |
| 3 | 76 | 3.82 | 97 | 150 | 375 | 570 | 2.75 |
| 4 | 102 | 4.84 | 123 | 150 | 375 | 750 | 4.65 |
| 2 | 51 | 2.76 | 70 | 300 | 750 | 400 | 1.75 |
| 3 | 76 | 3.94 | 100 | 300 | 750 | 570 | 2.85 |
| 4 | 102 | 4.96 | 126 | 300 | 750 | 750 | 4.75 |

LT1104

Beverage Transfer Hose

- Application:Suitable for the transfer of milk,juice,alcohol,and other beverages.

- Hose Construction

- Inner Tube:White EPDM synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Gray or blue EPDM synthetic rubber

- Temperature Range:-30°℃~100℃(-22°F~212°F)

- *The hose dimension,pressure and color can be customized based on the requirements

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 1/2 | 13 | 0.9 | 22.5 | 300 | 1200 | 130 | 0.35 |
| 5/8 | 16 | 1 | 26 | 300 | 1200 | 150 | 0.45 |
| 3/4 | 19 | 1.3 | 32 | 300 | 1200 | 180 | 0.6 |
| 1 | 25 | 1.5 | 38 | 300 | 1200 | 200 | 0.94 |
| 1-1/4 | 32 | 1.8 | 45 | 300 | 1200 | 250 | 1.2 |
| 1-1/2 | 38 | 2 | 52 | 300 | 1200 | 300 | 1.5 |
| 2 | 51 | 2.52 | 64 | 150 | 375 | 400 | 1.55 |
| 3 | 76 | 3.70 | 94 | 150 | 375 | 570 | 2.65 |
| 4 | 102 | 4.72 | 120 | 150 | 375 | 750 | 4.55 |
| 2 | 51 | 2.64 | 67 | 300 | 750 | 400 | 1.65 |
| 3 | 76 | 3.82 | 97 | 300 | 750 | 570 | 2.75 |
| 4 | 102 | 4.84 | 123 | 300 | 750 | 750 | 4.65 |