LT1306

GB/T 27571 UPE Super Abrasion Resistant Concrete Hose

- Application:Apply to construction machinery like pump truck to delivery concretes.Its service life is several times more than average products in the market,and the high saturation characteristic of UPE means that this product will not react with the alkaline substance in the concrete.

- Hose Construction

- Inner Tube:UPE and NR&SBR synthetic rubber

- Reinforcement:2~4 plies of sprial steel cord

- Outer Layer:black NR&SBR synthetic rubber(UPE layer is available)

- Temperature Range:-30°C~+82°C (-22°F~+180°F)

- *The hose dimension,pressure and color can be customized based on the requirements.

| I.D |  | 0.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.80 | 71 | 1250 | 3750 | 450 | 2.85 |
| 2.5 | 64 | 3.35 | 85 | 1250 | 3750 | 550 | 3.70 |
| 3 | 76 | 3.62 | 103 | 1250 | 3750 | 620 | 5.25 |
| 3.15 | 80 | 4.25 | 108 | 1250 | 3750 | 650 | 6.03 |
| 3.5 | 89 | 4.53 | 115 | 1250 | 3750 | 700 | 6.83 |
| 5 | 127 | 6.30 | 160 | 1250 | 3750 | 1050 | 11.00 |

LT1305

HG/T 2192 Bulk Materials Suction & Discharge Hose

- Application:widely apply to large-scale projects like mining & construction, tunnel project and construction machinery like shield machine and slotter etc. Depending on its features of super abrasion and corrosion resistant,this product also suitable to transfer pulverized coal, cement, and various corrosive chemicals.

- Hose Construction

- Inner Tube:black,abrasionresistant, antistatic NR&SBRsynthetic rubber or UPE

- Reinforcement:Multi-spiral high tensile synthetic fibersand helix spiral-wire

- Outer Layer:NR&SBR or EPDM synthetic rubber

- Temperature Range:-30°C~+82°C (-22°F~+180°F)

- *The hose dimension, pressure and color can be customizedbased on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.48 | 63 | 300 | 750 | 400 | 1.55 |
| 3 | 76 | 3.62 | 92 | 300 | 750 | 570 | 2.60 |
| 4 | 102 | 4.76 | 120 | 300 | 750 | 750 | 4.50 |
| 5 | 127 | 5.98 | 152 | 300 | 750 | 1000 | 6.50 |
| 6 | 152 | 7.76 | 197 | 300 | 750 | 1260 | 19.5 |

LT1402

Furnace Cooling Water Delivery Hose

- Application::Big diameter flexible hose specially designed for cooling water conveyin steel mills, glass plans and foundries with high cooling efficiency and long service life, suitable for high-temp and hot metal or glass splashing environment.

- Hose Construction

- Inner Tube:Black EPDM synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers and insulated spiral PP wire or helix spiral-wire

- Outer Layer:Black NBR&PVC fire retardant mixed rubber/thermal protective-layer and stainless steel armour

- Temperature Range:-40°C~+100°C(-40°F~+212°F);The cover radiant heat:540°C (1004°F)

- *The hose dimension, pressure and color can be customizedbased on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 3.03 | 77 | 300 | 750 | 420 | 1.85 |
| 3 | 76 | 4.06 | 103 | 300 | 750 | 590 | 2.90 |
| 4 | 102 | 5.20 | 132 | 300 | 750 | 770 | 5.30 |
| 5 | 127 | 5.87 | 149 | 300 | 750 | 950 | 6.45 |
| 6 | 152 | 6.81 | 173 | 300 | 750 | 1160 | 7.00 |
| 8 | 203 | 9.17 | 233 | 300 | 750 | 1400 | 15.00 |
| 10 | 254 | 11.30 | 287 | 300 | 750 | 1700 | 20.00 |