LT401L
EN12115 PTFE Low Pressure Multipurpose Hose
· Application:Widely apply to various industries like chemical, petroleum, iron and steel smelting, F&B and medication etc.The productis suitable to work under high temperature environment. Depending on its feature of super corrosion-resistant,even strong corrosion chemicals like sulfuric acid, hydrochloric acid and sulfur reactant could not react with it. It is alsoone of the best choices for food and medical industries.
· Hose Construction
· Inner Tube:PTFE and EPDM synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Black or blue EPDM or FKM synthetic rubber (UPE layer is available)
· Temperature Range:-55°C to 220°C (-67°F to 428°F)
· *The hose dimension, pressure and color can be customized based on the requirements.
	I.D
	O.D
	W.P
	Min.B.P
	W.T

	in
	mm
	in
	mm
	psi
	psi
	kg/m

	3/8
	10
	0.7
	19
	5075
	20300
	0.58

	1/2
	13
	0.9
	22.2
	4060
	16240
	0.61

	5/8
	16
	1.07
	27.2
	3625
	14500
	0.73

	3/4
	19
	1.2
	30.5
	3190
	12760
	0.95

	1
	25
	1.5
	38.4
	2465
	9860
	1.42

	1-1/4
	32
	1.8
	45.5
	1885
	7540
	1.72

	1-1/2
	38
	2.0
	51.5
	1305
	5220
	1.9

	2
	51
	2.80
	71
	300
	750
	2.05

	3
	76
	3.86
	98
	300
	750
	3.50

	4
	102
	5.00
	127
	300
	750
	5.50


LT401H
EN12115 PTFE High Pressure Multipurpose Hose
· Application:Widely apply to various industries like chemical, petroleum, iron and steel smelting, F&B and medication etc.The productis suitable to workunder high temperature environment. Dependingon its feature of super corrosion-resistant,even strong corrosion chemicals like sulfuric acid, hydrochloric acid and sulfur reactant could not react with it. It is alsoone of the best choices for food and medicalindustries.
· Hose Construction
· Inner Tube:PTFE and EPDM synthetic rubber
· Reinforcement:Two steel wire braids or four-ply of spiral steel wire
· Outer Layer:Black /red/yellow/blue oxygen, UV, and abrasion resistant NV or EPDM synthetic rubber (UPE layer is available)
· Temperature Range:-55°C to 220°C (-67°F to 428°F)
· *The hose dimension, pressure and color can be customized based on the requirements.
	I.D
	O.D
	W.P
	Min.B.P
	W.T

	in
	mm
	in
	mm
	psi
	psi
	kg/m

	3/8*2
	10
	0.83
	21
	6090
	24070
	0.82

	1/2*2
	13
	0.95
	24.2
	6090
	24070
	0.94

	5/8*2
	16
	1.15
	29.2
	6090
	24070
	1.25

	3/4*2
	19
	1.24
	31.5
	5510
	22040
	1.60

	1*2
	25
	1.56
	39.5
	5510
	22040
	1.93

	1-1/4*2
	32
	1.84
	46.8
	4785
	18850
	3.02

	1-1/2*2
	38
	2.21
	57
	4205
	16820
	3.57

	2*4
	51
	3.15
	80
	5000
	12500
	7.8

	3*4
	76
	4.25
	108
	5000
	12500
	12.0

	4*4
	102
	5.47
	139
	5000
	12500
	17.8


LT1202L
En 12115 Upe Low Pressure Multipurpose Hose
· Application:widely apply to industries like chemical,iron and steel smelting,construction,F&B,and medication etc.It is rarely reacting with any substance(oil,fats,corrosion chemicals etc.)because of its highly saturation materials.Its neutral taste and odor illustrates that it is safe to use in the F&B and medication industries.
· Hose Construction
· Inner Tube:UPE and EPDM synthetic rubber
· Reinforcement:multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Black or blue EPDM synthetic rubber (UPE layeris available)
· Temperature Range:-30°C to 82°C (-22°F to 180°F)
· *The hose dimension,pressure and color can be customized based on the requirements.
	I.D
	0.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	1/2
	13
	0.89
	22.5
	290
	870
	130
	0.34

	5/8
	16
	1.04
	26.5
	290
	870
	150
	0.44

	3/4
	19
	1.17
	29.7
	290
	870
	180
	0.52

	1
	25
	1.39
	35.2
	290
	870
	205
	0.52

	1-1/4
	32
	1.77
	45
	290
	870
	250
	0.95

	1-1/2
	38
	2.04
	52
	290
	870
	300
	1.2

	2
	51
	2.64
	67
	300
	750
	400
	1.65

	3
	76
	3.82
	97
	300
	750
	570
	2.75

	4
	102
	4.84
	123
	300
	750
	750
	4.65


LT1202H
EN12115 UPE High Pressure Multipurpose Hose
· Application:Widely apply to industries like chemical,iron and steel smelting,construction,F&B,and medication etc.It is rarely reacting with any substance (oil,fats,corrosion chemicals etc.)because of its highly saturation materials.Its neutral taste and odor illustrates that it is safe to use in the F&B and medical industries.
· Hose Construction
· Inner Tube:UPE and EPDM synthetic rubber
· Reinforcement:two steel wire braids or four-ply of spiral steel wire
· Outer Layer:black/red/yellow/blue oxygen,UV,and abrasion resistant NV or EPDM synthetic rubber(UPE layer is available)
· Temperature Range:30°℃~82℃(-22°F~180°F)
· *The hose dimension,pressure and color can be customized based on the requirements.
	I.D
	0.D
	W.P
	Min.B.P
	W.T

	in
	mm
	in
	mm
	psi
	psi
	kg/m

	3/8*2
	10
	0.75
	19
	5075
	20300
	0.58

	1/2*2
	13
	0.89
	22.2
	4060
	19140
	0.61

	5/8*2
	16
	1.07
	27.2
	3625
	15950
	0.73

	3/4*2
	19
	1.20
	30.5
	3190
	14500
	0.95

	1*2
	25
	1.52
	38.4
	2465
	12325
	1.42

	1-1/4*2
	32
	1.79
	45.5
	1885
	9425
	1.72

	1-1/2*2
	38
	2.03
	51.5
	1305
	5220
	1.9

	2*4
	51
	2.99
	76
	5000
	12500
	6.3

	3*4
	76
	4.09
	104
	5000
	12500
	10.5

	3-1/2*4
	89
	4.76
	121
	5000
	12500
	14

	4*4
	102
	5.28
	134
	5000
	12500
	16
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