LT401L

EN12115 PTFE Low Pressure Multipurpose Hose

- Application:Widely apply to various industries like chemical, petroleum, iron and steel smelting, F&B and medication etc.The productis suitable to work under high temperature environment. Depending on its feature of super corrosion-resistant,even strong corrosion chemicals like sulfuric acid, hydrochloric acid and sulfur reactant could not react with it. It is alsoone of the best choices for food and medical industries.

- Hose Construction

- Inner Tube:PTFE and EPDM synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Black or blue EPDM or FKM synthetic rubber (UPE layer is available)

- Temperature Range:-55°C to 220°C (-67°F to 428°F)

- *The hose dimension, pressure and color can be customized based on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | W.T |
| --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | kg/m |
| 3/8 | 10 | 0.7 | 19 | 5075 | 20300 | 0.58 |
| 1/2 | 13 | 0.9 | 22.2 | 4060 | 16240 | 0.61 |
| 5/8 | 16 | 1.07 | 27.2 | 3625 | 14500 | 0.73 |
| 3/4 | 19 | 1.2 | 30.5 | 3190 | 12760 | 0.95 |
| 1 | 25 | 1.5 | 38.4 | 2465 | 9860 | 1.42 |
| 1-1/4 | 32 | 1.8 | 45.5 | 1885 | 7540 | 1.72 |
| 1-1/2 | 38 | 2.0 | 51.5 | 1305 | 5220 | 1.9 |
| 2 | 51 | 2.80 | 71 | 300 | 750 | 2.05 |
| 3 | 76 | 3.86 | 98 | 300 | 750 | 3.50 |
| 4 | 102 | 5.00 | 127 | 300 | 750 | 5.50 |

LT401H

EN12115 PTFE High Pressure Multipurpose Hose

- Application:Widely apply to various industries like chemical, petroleum, iron and steel smelting, F&B and medication etc.The productis suitable to workunder high temperature environment. Dependingon its feature of super corrosion-resistant,even strong corrosion chemicals like sulfuric acid, hydrochloric acid and sulfur reactant could not react with it. It is alsoone of the best choices for food and medicalindustries.

- Hose Construction

- Inner Tube:PTFE and EPDM synthetic rubber

- Reinforcement:Two steel wire braids or four-ply of spiral steel wire

- Outer Layer:Black /red/yellow/blue oxygen, UV, and abrasion resistant NV or EPDM synthetic rubber (UPE layer is available)

- Temperature Range:-55°C to 220°C (-67°F to 428°F)

- *The hose dimension, pressure and color can be customized based on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | W.T |
| --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | kg/m |
| 3/8*2 | 10 | 0.83 | 21 | 6090 | 24070 | 0.82 |
| 1/2*2 | 13 | 0.95 | 24.2 | 6090 | 24070 | 0.94 |
| 5/8*2 | 16 | 1.15 | 29.2 | 6090 | 24070 | 1.25 |
| 3/4*2 | 19 | 1.24 | 31.5 | 5510 | 22040 | 1.60 |
| 1*2 | 25 | 1.56 | 39.5 | 5510 | 22040 | 1.93 |
| 1-1/4*2 | 32 | 1.84 | 46.8 | 4785 | 18850 | 3.02 |
| 1-1/2*2 | 38 | 2.21 | 57 | 4205 | 16820 | 3.57 |
| 2*4 | 51 | 3.15 | 80 | 5000 | 12500 | 7.8 |
| 3*4 | 76 | 4.25 | 108 | 5000 | 12500 | 12.0 |
| 4*4 | 102 | 5.47 | 139 | 5000 | 12500 | 17.8 |

LT1202L

En 12115 Upe Low Pressure Multipurpose Hose

- Application:widely apply to industries like chemical,iron and steel smelting,construction,F&B,and medication etc.It is rarely reacting with any substance(oil,fats,corrosion chemicals etc.)because of its highly saturation materials.Its neutral taste and odor illustrates that it is safe to use in the F&B and medication industries.

- Hose Construction

- Inner Tube:UPE and EPDM synthetic rubber

- Reinforcement:multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Black or blue EPDM synthetic rubber (UPE layeris available)

- Temperature Range:-30°C to 82°C (-22°F to 180°F)

- *The hose dimension,pressure and color can be customized based on the requirements.

| I.D |  | 0.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 1/2 | 13 | 0.89 | 22.5 | 290 | 870 | 130 | 0.34 |
| 5/8 | 16 | 1.04 | 26.5 | 290 | 870 | 150 | 0.44 |
| 3/4 | 19 | 1.17 | 29.7 | 290 | 870 | 180 | 0.52 |
| 1 | 25 | 1.39 | 35.2 | 290 | 870 | 205 | 0.52 |
| 1-1/4 | 32 | 1.77 | 45 | 290 | 870 | 250 | 0.95 |
| 1-1/2 | 38 | 2.04 | 52 | 290 | 870 | 300 | 1.2 |
| 2 | 51 | 2.64 | 67 | 300 | 750 | 400 | 1.65 |
| 3 | 76 | 3.82 | 97 | 300 | 750 | 570 | 2.75 |
| 4 | 102 | 4.84 | 123 | 300 | 750 | 750 | 4.65 |

LT1202H

EN12115 UPE High Pressure Multipurpose Hose

- Application:Widely apply to industries like chemical,iron and steel smelting,construction,F&B,and medication etc.It is rarely reacting with any substance (oil,fats,corrosion chemicals etc.)because of its highly saturation materials.Its neutral taste and odor illustrates that it is safe to use in the F&B and medical industries.

- Hose Construction

- Inner Tube:UPE and EPDM synthetic rubber

- Reinforcement:two steel wire braids or four-ply of spiral steel wire

- Outer Layer:black/red/yellow/blue oxygen,UV,and abrasion resistant NV or EPDM synthetic rubber(UPE layer is available)

- Temperature Range:30°℃~82℃(-22°F~180°F)

- *The hose dimension,pressure and color can be customized based on the requirements.

| I.D |  | 0.D |  | W.P | Min.B.P | W.T |
| --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | kg/m |
| 3/8*2 | 10 | 0.75 | 19 | 5075 | 20300 | 0.58 |
| 1/2*2 | 13 | 0.89 | 22.2 | 4060 | 19140 | 0.61 |
| 5/8*2 | 16 | 1.07 | 27.2 | 3625 | 15950 | 0.73 |
| 3/4*2 | 19 | 1.20 | 30.5 | 3190 | 14500 | 0.95 |
| 1*2 | 25 | 1.52 | 38.4 | 2465 | 12325 | 1.42 |
| 1-1/4*2 | 32 | 1.79 | 45.5 | 1885 | 9425 | 1.72 |
| 1-1/2*2 | 38 | 2.03 | 51.5 | 1305 | 5220 | 1.9 |
| 2*4 | 51 | 2.99 | 76 | 5000 | 12500 | 6.3 |
| 3*4 | 76 | 4.09 | 104 | 5000 | 12500 | 10.5 |
| 3-1/2*4 | 89 | 4.76 | 121 | 5000 | 12500 | 14 |
| 4*4 | 102 | 5.28 | 134 | 5000 | 12500 | 16 |