LT1203
SAE J1527 Marine Fuel Hose
· Application:Suitable for the transfer of fuel products such as gasoline,ethanol, 100% methanol,diesel,etc.
· Hose Construction
· Inner Tube:Black NBR synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire
· Outer Layer:  Black NBR and PVC fire retardant mixed rubber
· Temperature Range:-20℃~100℃(-4°F~212°F)
· *The hose dimension,pressure and color can be customized based on the requirements
	I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.76
	70
	75
	188
	400
	1.75

	3
	76
	3.74
	95
	75
	188
	570
	2.65

	4
	102
	4.84
	123
	75
	188
	750
	4.65

	5
	127
	6.06
	154
	75
	188
	1000
	6.50


LT1204
SAE J2006 Marine Wet Exhaust Hose
· Application:Could be used for engine water circulation, discharge lines, heat exchangers and wet exhaust connections.
· Hose Construction
· Inner Tube:Black NBR synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibers
· Outer Layer:Black NBR and PVC mixed rubber
· Temperature Range:-30°C to 100°C (-22°F to 212°F)
· *The hose dimension, pressure and color can be customized based on the requirements.
	[bookmark: _GoBack]I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.56
	65
	75
	188
	350
	1.60

	3
	76
	3.54
	90
	75
	188
	520
	2.60

	4
	102
	4.65
	118
	75
	188
	700
	4.50

	5
	127
	5.75
	146
	75
	188
	950
	6.00

	8
	203
	8.82
	224
	75
	188
	1400
	13.00


LT1213
ISO 1823 Petroleum Fuel Suction & Discharge Hose
· Application:Suitable for petroleum-based products transfer, such as gasoline, petroleum oil, ethanol,diesel, etc.
· Hose Construction
· Inner Tube:Black conductive NBR synthetic rubber
· Reinforcement:Multi-spiral high tensile synthetic fibersand helix spiral-wire
· Outer Layer:Black NBR and PVC mixed rubber
· Temperature Range:-30°C to 82°C (-22°F to 180°F)
· *The hose dimension, pressure and color can be customized based on the requirements.
	I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.68
	68
	300
	750
	400
	1.65

	3
	76
	3.78
	96
	300
	750
	570
	2.75

	4
	102
	4.80
	122
	300
	750
	750
	4.65

	6
	152
	6.97
	177
	300
	750
	1210
	6.80


LT1216
Hot Tar & Asphalt Suction & Discharge Hose
· Application:Suitable for petroleum-based products up to 356°F transfer, such as hot tar, asphalt, etc.
· Hose Construction
· Inner Tube:PTFE and FKM synthetic rubber
· Reinforcement:Multi-spiraled high tensile synthetic fibers and helix spiral-wire
· Outer Layer:Abrasion, oxygen, hot tar resistant, black synthetic rubber
· Temperature Range:-20°C to 180°C (-4°F to 356°F)
· *The hose dimension, pressure and color can be customizedbased on the requirements.
	I.D
	O.D
	W.P
	Min.B.P
	Min.B.R
	W.T

	in
	mm
	in
	mm
	psi
	psi
	mm
	kg/m

	2
	51
	2.80
	71
	300
	750
	430
	2.05

	3
	76
	3.86
	98
	300
	750
	600
	3.50

	4
	102
	5.00
	127
	300
	750
	780
	5.50



