LT1203

SAE J1527 Marine Fuel Hose

- Application:Suitable for the transfer of fuel products such as gasoline,ethanol, 100% methanol,diesel,etc.

- Hose Construction

- Inner Tube:Black NBR synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers and helix spiral-wire

- Outer Layer:  Black NBR and PVC fire retardant mixed rubber

- Temperature Range:-20℃~100℃(-4°F~212°F)

- *The hose dimension,pressure and color can be customized based on the requirements

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.76 | 70 | 75 | 188 | 400 | 1.75 |
| 3 | 76 | 3.74 | 95 | 75 | 188 | 570 | 2.65 |
| 4 | 102 | 4.84 | 123 | 75 | 188 | 750 | 4.65 |
| 5 | 127 | 6.06 | 154 | 75 | 188 | 1000 | 6.50 |

LT1204

SAE J2006 Marine Wet Exhaust Hose

- Application:Could be used for engine water circulation, discharge lines, heat exchangers and wet exhaust connections.

- Hose Construction

- Inner Tube:Black NBR synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibers

- Outer Layer:Black NBR and PVC mixed rubber

- Temperature Range:-30°C to 100°C (-22°F to 212°F)

- *The hose dimension, pressure and color can be customized based on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.56 | 65 | 75 | 188 | 350 | 1.60 |
| 3 | 76 | 3.54 | 90 | 75 | 188 | 520 | 2.60 |
| 4 | 102 | 4.65 | 118 | 75 | 188 | 700 | 4.50 |
| 5 | 127 | 5.75 | 146 | 75 | 188 | 950 | 6.00 |
| 8 | 203 | 8.82 | 224 | 75 | 188 | 1400 | 13.00 |

LT1213

ISO 1823 Petroleum Fuel Suction & Discharge Hose

- Application:Suitable for petroleum-based products transfer, such as gasoline, petroleum oil, ethanol,diesel, etc.

- Hose Construction

- Inner Tube:Black conductive NBR synthetic rubber

- Reinforcement:Multi-spiral high tensile synthetic fibersand helix spiral-wire

- Outer Layer:Black NBR and PVC mixed rubber

- Temperature Range:-30°C to 82°C (-22°F to 180°F)

- *The hose dimension, pressure and color can be customized based on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.68 | 68 | 300 | 750 | 400 | 1.65 |
| 3 | 76 | 3.78 | 96 | 300 | 750 | 570 | 2.75 |
| 4 | 102 | 4.80 | 122 | 300 | 750 | 750 | 4.65 |
| 6 | 152 | 6.97 | 177 | 300 | 750 | 1210 | 6.80 |

LT1216

Hot Tar & Asphalt Suction & Discharge Hose

- Application:Suitable for petroleum-based products up to 356°F transfer, such as hot tar, asphalt, etc.

- Hose Construction

- Inner Tube:PTFE and FKM synthetic rubber

- Reinforcement:Multi-spiraled high tensile synthetic fibers and helix spiral-wire

- Outer Layer:Abrasion, oxygen, hot tar resistant, black synthetic rubber

- Temperature Range:-20°C to 180°C (-4°F to 356°F)

- *The hose dimension, pressure and color can be customizedbased on the requirements.

| I.D |  | O.D |  | W.P | Min.B.P | Min.B.R | W.T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | psi | psi | mm | kg/m |
| 2 | 51 | 2.80 | 71 | 300 | 750 | 430 | 2.05 |
| 3 | 76 | 3.86 | 98 | 300 | 750 | 600 | 3.50 |
| 4 | 102 | 5.00 | 127 | 300 | 750 | 780 | 5.50 |