LT305

17K Jumper Hose

- Inner Tube:UPE or PTFE (thickness 4.0mm)

- Reinforcement:Synthetic rubber, polyester fiber braiding and high-strength ultra-flexible copper-coated steel wire

- Outer Cover:Wear-resistant weather-resistant synthetic rubber + stainless steel armor

- Temperature Range:-30°C~+100°C (-22°F~+212°F)

- Compliance Standard:API 17K Third Edition

- Application:Features high pressure, lightweight, and long life characteristics, with superior corrosion resistance compared to traditional steel hose, can replace steel hose for deep-sea oil and gas transportation.

| I.D. (in) | O.D. (mm) | O.D. (mm) | W.P.(Bar) | T.P. (Bar) | B.P.(Bar) | Min.B.R.（m） | Weight per meter of the hose in seawater.（kg/m） | hose length（m） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 | 76 | 130 | 232 | 348 | 580 | 1.2 | 4 | 77 |
| 8 | 203 | 275 | 93 | 139.5 | 232.5 | 2.1 | 3 | 77 |
| 12 | 304 | 375 | 18 | 27 | 45 | 2.8 | 108 | 77 |
| 16 | 406 | 485 | 50 | 75 | 125 | 3.2 | 200 | 77 |

LT301 F

Super Abrasion Resistant Frac Hose

- Hose Construction

- Inner Tube:UPE and synthetic rubber

- Reinforcement:multi-spiraled high tensile super flexible steel wire

- Outer Layer:abrasion and weather resistant synthetic rubber

- Temperature Range:-29°C~+100°C (-20°F~+212°F)

- Connector:intgral union,integral flange,or other connector types

- Application:Flexible line using for delivery water-based,oil-based,acid-based and foam fracturing fluids under high pressure in acid,sand and hydraulic fracturing works

| Size | I.D. | 0.D. | W.P. | T.P. | Min.B.R. |  | W.T |  | Volume |  | Connector W.T |  | Connection Type |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| inch | mm | mm | Psi | Psi | m | ft | kg/m | Ib/ft | bbl/min | m3/min | kg | Ib/set |  |
| 2" | 32 | 81 | 15000 | 22500 | 1.2 | 3.94 | 11.5 | 7.7 | 4.5 | 0.72 | 25 | 55 | 2"FIG 1502 HammerUnion or 21/16"15K APIflange |
|  | 44 | 95 | 15000 | 22500 | 1.4 | 4.59 | 18 | 12 | 9 | 1.46 | 45 | 99 | 3"FIG1502 Hammer Union or 31/16"15KAPlflange" |
|  | 51 | 107 | 15000 | 22500 | 1.4 | 4.59 | 20 | 13 | 12 | 1.91 | 59 | 130 |  |
| 2.5" | 58 | 122 | 15000 | 22500 | 1.5 | 4.92 | 24 | 16 | 15 | 2.39 | 61 | 134 |  |
|  | 64 | 126 | 15000 | 22500 | 1.5 | 4.92 | 27 | 18 | 18.5 | 2.90 | 75 | 165 |  |
| 3" | 69 | 135 | 15000 | 22500 | 1.6 | 5.25 | 30 | 20 | 21.5 | 3.42 | 91 | 201 |  |
|  | 76 | 145 | 15000 | 22500 | 1.6 | 5.25 | 35 | 24 | 26 | 4.13 | 102 | 225 |  |
| 4" | 89 | 164 | 15000 | 22500 | 2.0 | 6.56 | 52 | 35 | 36 | 5.72 | 132 | 291 | 4"FIG1502 Hammer Union or 41/16"15KAPlflange |
|  | 102 | 179 | 15000 | 22500 | 2.0 | 6.56 | 60 | 40 | 47 | 7.47 | 154 | 340 |  |
| 5" | 120 | 208 | 15000 | 22500 | 2.1 | 6.89 | 80 | 54 | 65 | 10.34 | 402 | 886 | 51/8"15KAPIflange |
|  | 127 | 216 | 15000 | 22500 | 2.1 | 6.89 | 86 | 58 | 73 | 11.61 | 407 | 897 |  |
| 5.5" | 140 | 243 | 15000 | 22500 | 2.2 | 7.22 | 110 | 74 | 88.5 | 14.07 | 653 | 1440 | 71/16"15KAPI flange |
| 6" | 152 | 255 | 15000 | 22500 | 2.3 | 7.54 | 125 | 84 | 104.5 | 16.62 | 703 | 1550 |  |
| 2" | 51 | 112 | 20000 | 30000 | 1.5 | 4.92 | 26 | 17 | 12 | 1.91 | 78 | 172 | 2"FIG 2002Hammer Union or 31/16"20KAPI flange |
| 2.5" | 64 | 133 | 20000 | 30000 | 1.6 | 5.25 | 36 | 24 | 18.5 | 2.90 | 103 | 227 | 3"FIG 2002Hammer Union or 31/16"20KAPlflange |
| 3" | 76 | 159 | 20000 | 30000 | 1.9 | 6.23 | 57 | 38 | 26 | 4.13 | 135 | 298 | 3"FIG 2002Hammer Union or 31/16"20KAPlflange |
| 4" | 102 | 202 | 20000 | 30000 | 2.1 | 6.89 | 94 | 63 | 47 | 7.47 | 400 | 882 | 41/16"20KAPI flange |

Remark:According to the customer'srequriements,the I.D.of all the above sizes of hose assemblies can be made into full bore I.D.or non-full bore l.D.(A full bore hose assembly's effective flow I.D. is at least 95% of its nominal I.D.)The flow rate is calculated at a flow velocity of 50ft/s;LETONE recommends that the working flow velocity should not exceed 40ft/s.

LT304

Multi-Purpose Crude Oil Hose

- Hose Construction

- Inner Tube:Polymer composites

- Reinforcement:Multi-spiraled high tensile texile cords and highly flexible steel helix wire

- Outer Layer:Synthetic rubber

- Temperature Range:-40°C~+180°C (-40°F~+356°F)

- *The hose dimension, pressure and color can be customizedbased on the requirements.

- Application:The hose is suitable for delivering petroleum products such as fuel oil, crude oil, gasoline, etc. The hose inner layer is made of polymer composites, which makes the hose with strong corrosion resistance and high lubrication characteristics. Its excellent chemical stability prevents it from reacting with chemical substances in petroleum products,ensuring safe and efficient transportation of the medium.

| I.D. |  | W.P | Safety Factor |
| --- | --- | --- | --- |
| in. | mm | MPa |  |
| 2 | 51 | 2-35 | 2.5times |
| 2 1/2 | 63 | 2-35 | 2.5times |
| 3 | 76 | 2-35 | 2.5times |
| 3 1/2 | 90 | 2-35 | 2.5times |
| 4 | 102 | 2-35 | 2.5times |
| 5 | 127 | 2-35 | 2.5times |
| 6 | 152 | 2-35 | 2.5times |

Note: Actual parameters are subject to the latest catalog.

LT301 C

APISpec. 7K FSL0 |ABS High Pressure Cementing Hose

- Hose Construction

- Inner Tube:UPE and synthetic rubber or HNBR

- Reinforcement:Multi-spiraled high tensile super flexible steel wire

- Outer Layer:Abrasion and weather resistant synthetic rubber

- Temperature Range:-20°C~+121°C (-4°F~+250°F)

- Connector:Integral union or integral flange

- Application:Flexible connection in the manifold for delivery water-based and oil-based cement slurries under high pressure.

| Pressure Level | I.D. | O.D. | W.P. | P.P. | Min.B.P. | Min.B.R. | Weight |
| --- | --- | --- | --- | --- | --- | --- | --- |
| psi | in. | mm | psi | psi | psi | mm | kg/m |
| 10000 | 2 | 83 | 10000 | 15000 | 22500 | 1000 | 10.8 |
|  | 2 1/2 | 98 | 10000 | 15000 | 22500 | 1000 | 19.4 |
|  | 3 | 129 | 10000 | 15000 | 22500 | 1400 | 28 |
|  | 3 1/2 | 137 | 10000 | 15000 | 22500 | 1400 | 33 |
|  | 4 | 154 | 10000 | 15000 | 22500 | 1600 | 38.5 |
|  | 5 | 154 | 10000 | 15000 | 22500 | 1800 | 56.5 |
| 15000 | 2 | 101 | 15000 | 22500 | 33750 | 1200 | 20.5 |
|  | 3 | 125 | 15000 | 22500 | 33750 | 1500 | 36 |
| 20000 | 2 | 106 | 20000 | 30000 | 45000 | 1500 | 24 |
|  | 3 | 142 | 20000 | 30000 | 45000 | 1700 | 44 |

Note: Actual parameters are subject to the latest catalog.

LT301 D

API Spec. 7K-Rotary Drilling And Vibrator Hose

- Hose Construction

- Inner Tube:Synthetic rubber/HNBR/UPE/PTFE

- Reinforcement:Multi-spiraled high tensile super flexible steel wire

- Outer Layer:Abrasion and weather resistant synthetic rubber

- Temperature Range:-20°C~+121°C (-4°F~+250°F)

- Connector:Integral union, integral flange, or other connector types Full bore can be customized based on the requirements

- Full bore hose inner layer can be customized

- Application:Flexible connection between the upper end of the riser and the top drive/rotating assembly, and between the pump and the lower end of the riser in drilling, cementing, and well workover operations, for high-pressure mud pumping in oil drilling and exploration work

| Pressure Level | I.D. | O.D. | W.P. | P.P. | Min.B.P. | Min.B.R. | Weight |
| --- | --- | --- | --- | --- | --- | --- | --- |
| psi | in. | mm | psi | psi | psi | mm | kg/m |
| 1500 Grade A | 2 | 68 | 1500 | 2250 | 3750 | 800 | 4.3 |
|  | 2 1/2 | 84 | 1500 | 2250 | 3750 | 800 | 5.6 |
| 2000 Grade B | 2 | 68 | 2000 | 3000 | 5000 | 800 | 4.3 |
|  | 2 1/2 | 84 | 2000 | 3000 | 5000 | 800 | 5.6 |
|  | 3 | 97 | 2000 | 3000 | 5000 | 950 | 6.5 |
|  | 3 1/2 | 113 | 2000 | 3000 | 5000 | 1000 | 8.5 |
|  | 4 | 127 | 2000 | 3000 | 5000 | 1000 | 10.4 |
|  | 5 | 157 | 2000 | 3000 | 5000 | 1200 | 14.0 |
|  | 6 | 183 | 2000 | 3000 | 5000 | 1300 | 18.0 |
| 4000 Grade C | 2 | 72 | 4000 | 6000 | 10000 | 800 | 6.4 |
|  | 2 1/2 | 87 | 4000 | 6000 | 10000 | 800 | 8.7 |
|  | 3 | 102 | 4000 | 6000 | 10000 | 1000 | 11.1 |
|  | 3 1/2 | 119 | 4000 | 6000 | 10000 | 1200 | 14.4 |
|  | 4 | 132 | 4000 | 6000 | 10000 | 1200 | 16.0 |
|  | 5 | 162 | 4000 | 6000 | 10000 | 1400 | 24.5 |
|  | 6 | 194 | 4000 | 6000 | 10000 | 1500 | 33 |
| 5000 Grade D | 2 | 75 | 5000 | 7500 | 12500 | 800 | 6.4 |
|  | 2 1/2 | 90 | 5000 | 7500 | 12500 | 800 | 8.7 |
|  | 3 | 104 | 5000 | 7500 | 12500 | 1000 | 11.1 |
|  | 3 1/2 | 121 | 5000 | 7500 | 12500 | 1200 | 14.4 |
|  | 4 | 134 | 5000 | 7500 | 12500 | 1200 | 16.0 |
|  | 5 | 167 | 5000 | 7500 | 12500 | 1400 | 24.5 |
|  | 6 | 196 | 5000 | 7500 | 12500 | 1600 | 33 |
| 7500 Grade E | 2 | 77 | 7500 | 11250 | 18750 | 900 | 8.5 |
|  | 2 1/2 | 94 | 7500 | 11250 | 18750 | 1000 | 10.5 |
|  | 3 | 110 | 7500 | 11250 | 18750 | 1000 | 18.5 |
|  | 3 1/2 | 128 | 7500 | 11250 | 18750 | 1200 | 20 |
|  | 4 | 150 | 7500 | 11250 | 18750 | 1400 | 30 |
|  | 5 | 183 | 7500 | 11250 | 18750 | 1600 | 49 |
|  | 6 | 212 | 7500 | 11250 | 18750 | 1600 | 60 |

Note: Actual parameters are subject to the latest catalog.

LT302

API 16C Series-Flexible Choke and Kill Line

- Hose Construction

- Inner Tube:HNBR/UPE

- Bore Type:Full bore

- Reinforcement:Multi-spiraled high tensile super flexible steel wire

- Outer Layer:High temperature and fire resistant synthetic rubber (resistant to 704°C open fire for 30 minutes)

- Outer Protection Layer:Stainless steel armor

- Temperature Range:-29°C~+121°C (-20°F~+250°F)

- Connector:Integral hammer union or integral flange

- Application:Flexible connection in the chock and kill manifolds for delivery oil-gas mixture that containing hydrogen sulfide (H2S) and other dangerous gases and various water-based, oil-based and foam killing fluids under high pressure.

| Pressure Level | I.D. | 0.D. | W.P. | P.P. | Min. B.P. | Min.B.R. | Weight |
| --- | --- | --- | --- | --- | --- | --- | --- |
| psi | in. | mm | psi | psi | psi | mm | kg/m |
| 5000 | 2 | 89 | 5000 | 7500 | 11250 | 1000 | 9.5 |
|  | 3 | 115 | 5000 | 7500 | 11250 | 1200 | 14.8 |
|  | 3 1/2 | 133 | 5000 | 7500 | 11250 | 1400 | 20 |
|  | 4 | 147 | 5000 | 7500 | 11250 | 1600 | 30 |
| 10000 | 2 | 96 | 10000 | 15000 | 22500 | 1200 | 15 |
|  | 2 1/2 | 126 | 10000 | 15000 | 22500 | 1600 | 25 |
|  | 3 | 140 | 10000 | 15000 | 22500 | 1600 | 33 |
|  | 4 | 167 | 10000 | 15000 | 22500 | 1800 | 52 |
| 15000 | 2 | 101 | 15000 | 22500 | 33750 | 1400 | 21 |
|  | 3 | 141 | 15000 | 22500 | 33750 | 1600 | 33 |
|  | 4 | 171 | 15000 | 22500 | 33750 | 2000 | 56 |

Note: Actual parameters are subject to the latest catalog.

LT303

API 16D Series-BOP Control Hose

- Hose Construction

- Inner Tube:NBR

- Tube Type:Full bore

- Reinforcement:4 plies of spiraled high tensile super flexible steel wire

- Outer Layer:High temperature and fire resistant synthetic rubber

- Protection Layer:Stainless steel armor

- Temperature Range:-40°C~+100°C (-40°F~+212°F) Fire resistance meets API Spec. 16D, 704°Cx5min

- Application:Hydraulic control line for remotely control the blowout preventer (BOP) at high pressure.

| I.D. | W.P. | P.P. | Min. B.P. | Min. B.R. | Weight |
| --- | --- | --- | --- | --- | --- |
| (in.) | (psi) | (psi) | (psi) | (mm) | (kg/m) |
| 1/2 | 5000 | 7500 | 15000 | 300 | 1.9 |
| 3/4 | 5000 | 7500 | 15000 | 400 | 2.7 |
| 1 | 5000 | 7500 | 15000 | 500 | 3.6 |
| 1 1/2 | 5000 | 7500 | 15000 | 700 | 5.3 |
| 2 | 5000 | 7500 | 15000 | 800 | 7.2 |

Note: Actual parameters are subject to the latest catalog.